## Slide 1
Figure 1. Secondary electron plan view micrographs of HCC and HCC+CIP specimens

## Slide 2
Figure 2. Comparative of released load fraction from porous PCL films and HHC+CIP systems. The porous PCL films were applied on a model substrate (glass) with 0.57 g of CIP. The HHC+CIP system was loaded with 1.03 mg of the drug.

## Slide 3
Figure 3. Hydrogen evolution for CIP-free and CIP-loaded HHC on Mg3Zn0.4Ca alloy during immersion in inorganic α-MEM at 37ºC under flow of CO2.

## Slide 4
10 µm
b)
c)
PEO hydratated
Crevice
10 µm
Figure 4. Secondary (a) and backscattered (b, c) electron micrographs of HHC+CIP: a) view of the PCL layer defects at the specimen edge; b, c) cross-sectional views following 24 h of immersion in inorganic α-MEM at 37ºC.
Corrosion products
PEO
PEO
200 µm
PEO
a)
Mg3Zn0.4Ca alloy
PCL

## Slide 5
Mg3Zn0.4Ca/PEO
Discharge channel
Figure 5. TEM micrographs of the barrier layer of the PEO coating on Mg3Zn0.4Ca alloy
Mg3Zn0.4Ca
Barrier layer of PEO

## Slide 6
-100.0
-100.0
-100.0
-100.0
-100.0
-100.0-100.0
-100.0
-100.0
-100.0
-1500
-1000
-500
0
500
1000
1500
Y µm,
-100.0
-75.0
-50.0
-25.0
0.0
25.0
50.0
75.0
100.0
i, µA/cm2
100.0
100.0
100.0
0.0
100.0
10
100.0
0.0 100.0
100.0
100.0
100.00.0
100.0
100.0
100.0
100.0
100.0100.0 100.0
100.0 100.0
100.0
100.0
100.0 100.0
100.0
100.0
100.0
100.0
-1500
-1000
-500
0
500
1000
1500
Y, µm
-100.0
-75.0
-50.0
-25.0
0.0
25.0
50.0
75.0
100.0
i, µA/cm2
100.0
50.0
25.0
25.0
25.0
50.0
100.0
25.0
25.0
25.0
50.0
50.
25.0
75.0
100.0
25.0
75.0
100.0
50.0
75.0
25.0
50.0
75.0
50.0
25.0
-1500
-1000
-500
0
500
1000
1500
Y, µm
-100.0
-75.0
-50.0
-25.0
0.0
25.0
50.0
75.0
100.0
i, µA/cm2
-1500
-1000
-500 0
X, µm
500
1000
1500
-1500
-1000
-500 0
X, µm
500
1000
1500
-1500
-1000
-500 0
X, µm
500
1000
1500
1 h
12 h
24 h
37.5
12.5
37.5
37.5
37.5
37.5
12.5
37.5 37.5
37.5
37.5 37.5
12.5
37.5
37.5
37.5
37.5
12.5
12.5
-1500
-1000
-500
0
500
1000
1500
Y, m
-100.0
-75.0
-50.0
-25.0
0.0
25.0
50.0
75.0
100.0
i, µA/cm2
12.5
-12.5
12.5
12.5
12.5
12.5
12.5
12.5
-12.5
-12.5
12.5
12.5
12.5
12.5
-1500
1000 12.5
-1000
-500
0
500
1500
Y, µm
-100.0
-75.0
-50.0
-25.0
0.0
25.0
50.0
75.0
100.0
i, µ A/cm2
-20.8
4.2
4.2
-20.8
-20.8
4.2
4.2
4.2
-20.8
-20.8
4.2
4.2
4.2
4.2
4.2
4.2
4.2
4.2
4.2
4.2
4.2
4.2
-1500
-1000
-500
0
500
1000
1500
Y, µm
-100.0
-75.0
-50.0
-25.0
0.0
25.0
50.0
75.0
100.0
i, µA/cm2
-1500
-1000
-500 0
X, µm
500
1000
1500
-1500
-1000
-500 0
X, µm
500
1000
1500
-1500
-1000
-500 0
X, µm
500
1000
1500
HHC
HHC+CIP
Figure 6. Optical micrographs and SVET current density distribution on CIP-free and CIP-loaded HCC system after 1, 12 and 24 h of immersion in α-MEM at 37ºC. The red rectangle in each optical micrograph indicates the precise location of local pH and H2 mapping (3 × 3 mm)..

## Slide 7
7.95
8.03
7
8.0
8.03
7.95
7.95
7.95
7.95
7.9 5.95 7.95
-1000
-500
500
1000
0
-1000
-500
0
500
1000
Y, µm
7.80
7.88
7.95
8.03
8.10
8.18
8.25
8.33
8.40
pH
1.88
1.88
1.88
-1000
-500
500
1000
0
-1000
-500
0
500
1000
Y, µm
1.00
1.88
2.75
3.63
4.50
5.38
6.25
7.13
8.00
H2, µmol/L
1 h
7.95
7
7.88 .88
7.88
7.88
7.95
7.95
7.95
7.95
-1000
-500
0
500
1000
Y µm
7.80
7.88
7.95
8.03
8.10
8.18
8.25
8.33
8.40
pH
.31
2
2.31 .31
2.31
2.31
2.60
2.31
2.31
2.75
3.63
2.60
2.31
2.31
2.31
2.31
2.60
-1000
-500
0
500
1000
Y, µm
1.00
1.88
2.75
3.63
4.50
5.38
6.25
7.13
8.00
H2, µmol/L
6 h
0
500
1000
-1000
-500
0
500
1000
X, µm
X, µm
X, µm
X, µm
8.33
.25
8.25
8.25
8.33
8.33
8.33
8.33
8.25
-500
.25
-1000
0
500
1000
7.80
7.88
7.95
8.03
8.10
8.18
8.25
8.33
8.40
2.17
3.63
2.02
2.02
2.02
2.02 2.02
2.02
2.17 2.02
2.17
2.17
2.02
1000 2.75
-1000
-500
0
500
1.00
1.88
2.75
3.63
4.50
5.38
6.25
7.13
8.00
24 h
-1000
-500
0
500
1000
-1000
-500
0
500
1000
Y µm
Y, µm
X, µm
X, µm
pH
H2, µmol/L
a)
d)
g)
b)
e)
h)
c)
f)
i)
Figure 7. (a, d, g) The visual appearances, (b, c, h) local pH distribution and (c, f , i) local dissolved H2 concentration for HHC after 1 h, 6 h and 24 h of immersion in inorganic α-MEM at 37ºC. The red rectangle in each optical micrograph indicates the precise location of local pH and H2 mapping (3 × 3 mm).

## Slide 8
3.19
1.88
1.88 1.88
2.90
1.88
1.291.291.29
1.29
1.88
1.88
-1500 -1000
-500
500
1000 1500
-1500
0
-1000
-500
0
500
1000
1500
1.00
1.88
2.75
3.63
4.50
5.38
6.25
7.13
8.00
8.33
8.25
8.25
8.25
8.33
8.33
8.25
-1500
-1000
-500
500
1000 1500
-1500
0
-1000
-500
0
500
1000
1500
7.80
7.88
7.95
8.03
8.10
8.18
8.25
8.33
8.40
pH
1 h
7
7.88
7.88
7.8
7.88 .88
7.88
7.88
7.88
7.88
7.88
7.88
-1000
-500
0
500
1000
1500
7.88
7.95
8.03
8.10
8.18
8.25
8.33
8.40
pH
6.25
4.50
2.75
2.75
3.63
3.63
2.75
2.75 2.75
2.75
2.75
-1000
-500
0
500
1000
1500
1.00
1.88
2.75
3.63
4.50
5.38
6.25
7.13
8.00
6 h
7.80
-1500
-1500
-1500
-1500
-1000
-500
0
500
1000
1500
-1000
-500
0
500
1000
1500
.41
2.76
3.41
3.41
4.69
5.33
4.05 5.98
4.69
2.76
2.76 2.76
3.41
3.41
5.33
6.62
4.05
2.76
2.76
3.41
-1000
-500
0
500
1000
1500
2.76
3.41
4.05
4.69
5.33
5.98
6.62
7.26
7.95
.88
7.88
8.03
7.88
7.95
8.03
7.88
7.95
7.95
7.88
-1000
-500
0
500
1000
1500
7.88
7.95
8.03
8.10
8.18
8.25
8.33
8.40
pH
24 h
7.95
500
2.76
0
2.76
1000
7.80
2.12
-1500
-1500
-1500
-1500
-1000
-500
0
1000
1500
-1000
-500
500
1500
Y, µm
Y, µm
H2, µmol/L
Y µm
Y, µm
H2, µmol/L
X, µm
X, µm
X, µm
X, µm
Y µm
Y, µm
X, µm
X, µm
a)
d)
g)
b)
e)
h)
c)
f)
i)
H2, µmol/L
Figure 8. (a, d, g) The visual appearances, (b, c, h) distributions of local pH and (c, f ,i ) H2 concentration of HHC+CIP in inorganic α-MEM at 37ºC after 1, 6 and 24 h. The red rectangle in each optical micrograph indicates the precise location of local pH and H2 mapping (3 × 3 mm).

## Slide 9
Figure 9. Regulation of pH by CIP zwitterion release
pH = 8.3
pH = 7.9
pKa = 8.9
pKa = 5.9

## Slide 10
100 µm
50 µm
20 µm
100 µm
30 µm
10 µm
a)
b)
c)
d)
e)
f)
HHC
HHC+CIP
Crevice
Corrosion products
Crevice
Crevice
PEO hydratated
Crevice
PEO hydratated
PEO hydratated
Figure 10. Backscattered electron cross-sectional images of (a-c) HHC and (d-f) HHC+CIP after local pH and local H2 concentration measurements in inorganic α-MEM at 37ºC.
Corrosion products

## Slide 11
NH
OH
OH
(H2O)
CH-CH
CH-CH
O=C
O=C
C-C
C-H
N-C
C-H
C-O
O=C
C=C
PCL
Ciprofloxacin
C-O
Figure 11. FTIR spectra of ciprofloxacin (red), PCL (black) layer in as-received HHC specimen and PCL+CIP layer in HHC+CIP specimens (blue) after 48 h of immersion in inorganic α-MEM solution.
C-H
C-H
C-H

## Slide 12
Figure 12. Evolution of (a) total modulus of impedance at low frequencies (0.1 Hz) and (b) pH for HHC and HHC+CIP systems during immersion in inorganic α-MEM at 37ºC.
a)
b)
1 cm
1 cm

## Slide 13
Point/ EDS (at. %) | C | O | Na | Mg | Si | P | Cl | K | Ca | N
1 | 59.6 | 33.3 | 0.1 | 0.6 | 2.7 | 0.0 | 0.0 | 3.3 | 0.4 | -
2 | 52.5 | 32.4 | 0.1 | 0.5 | - | 2.5 | 0.0 | 0.0 | 3.1 | 8.6
1
2
100 µm
20 µm
100 µm
20 µm
b)
c)
d)
e)
f)
HHC
HHC+CIP
Figure 13. (a) The evolution of resistance of the layers of CIP-free and CIP-loaded HHC system during immersion; (b-e) secondary electron images of (b, c) HHC and (d, e) HHC+CIP specimens after EIS measurements at 48 h; (f) local EDS analysis (at. %) of (c, e) images.
a)

## Slide 14
Supplementary Figure 1. (a) Absorption spectra and (b) standard curve of ciprofloxacin at different concentrations in inorganic α-MEM at 25ºC.

## Slide 15
HHC
HHC+CIP
a)
b)
c)
d)
e)
f)
Supplementary Figure 2. (a, d) Optical micrographs, (b, e) 3D rendering and (c ,f) -variation of surface topography in 3D of (a-c) drug-free and (d-f) CIP-loaded HHC systems.
50 µm
50 µm

## Slide 16
Supplementary Figure 3. Zwitterionic chelate complex of ciprofloxacin with Mg2+ and Ca2+ cations (M) released by PEO coating and Mg alloy.

## Slide 17
Z” (Ω·cm2)
Z” (Ω·cm2)
|Z | (Ω·cm2)
Frequency (Hz)
Frequency (Hz)
Theta (o)
HHC_1h
HHC_24h
HHC+CIP_1h
HHC+CIP_24h
Supplementary Figure 3. Nyquist and Bode diagrams for CIP-free and CIP-loaded HHC on Mg3Zn04Ca alloy after 1 h and 24 h of immersion in inorganic α-MEM solution at 37oC.
Rel
CPE1
R2
CPE2
R3
CPE3
R1