- Table 1. Surface parameters of drug-free and CIP-loaded hybrid hierarchical coating.

| HHC system | Pore size (µm) |  | Surface pore population density (pore/mm2)· 103 | Contact angle (º) | Sa (µm) | S10z (µm) |
| --- | --- | --- | --- | --- | --- | --- |
| HHC | 8.5 ± 2.8 | 298 |  | 88.9 ± 5.0 | 0.6 ± 0.2 | 7.2 ± 3.7 |
| HHC +CIP | 12.2 ± 1.1 | 76 |  | 96.1 ± 3.0 | 0.5 ± 0.1 | 5.2 ± 1.5 |

Table S1. Fitted electrical parameters of EIS spectra of HHC and HHC+CIP specimens after 1 h and 24 h of immersion in inorganic α-MEM solution at 37oC.

| HHC system | Rel (Ω·cm2) | CPE1 (µS·sn·cm-2) | n1 | R1 (Ω·cm2) | CPE2 (µS·sn·cm-2) | n2 | R2 (Ω·cm2) | CPE3 (mS·sn·cm-2) | n3 | R3 (Ω·cm2) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HHC_1h | 61.63 | 0.02 | 0.78 | 7105 | 0.36 | 0.56 | 55877 | 5.53 | 0.80 | 57642 |
| HHC_24h | 61.63 | 0.02 | 0.78 | 4426 | 1.34 | 0.69 | 9154 | 28.48 | 0.69 | 4706 |
| HHC+CIP_1h | 61.63 | 0.21 | 0.71 | 528.6 | 0.24 | 0.81 | 38366 | 5.00 | 0.90 | 26579 |
| HHC+CIP_24h | 61.63 | 0.36 | 0.78 | 120 | 1.44 | 0.77 | 40246 | 12.20 | 0.76 | 28420 |