Table 1. Local EDS analysis (at.%) of conventional (C) and DMLS (AM) substrates after etching in Keller solution, as per locations in Figure 1.

| Specimen/ Location |  | Na | Mg | Al | Si | P | S | K | Ti | Ca | Zn | O | V | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C | Area | - | - | 9.6 | - | - | - | - | 87.3 | - | - | - | 3.1 | - |
| AM | 1 | - | - | 8.2 | - | - | - | - | 92.1 | - | - | - | 5.6 | 0.7 |
|  | 2 | - | - | 6.6 | 0.09 | - | - | - | 93.5 | - | - | - | 3.8 | 0.1 |
|  | 3 | - | - | 7.3 | - | - | - | - | 91.8 | - | - | - | 5.8 | 0.8 |

Table 2. Local EDS analysis (at.%) of conventional (C) and DMLS (AM) substrates with flash-PEO (60s) and PEO (300s) coatings, as per locations in Figure 3.

| Specimen/ Location |  | Na | Mg | Al | Si | P | S | K | Ti | Ca | Zn | O | V | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AM-300s (SS) | Plan view area | 0.8 | 2.5 | 0.7 | 14.1 | 4.1 | 1.0 | 0.2 | 5.5 | 1 | - | 70.2 | - | - |
| C-300s (SS) |  | - | - | 0.5 | 11.6 | 3.7 | 4.6 | - | 3.4 | 5.6 | - | 70.6 | - | - |
| AM- 300s |  | 0.8 | 2.5 | 0.7 | 13.8 | 4.1 | 0.9 | 0.2 | 5.4 | 1 | - | 70.4 | 0.2 | - |
| AM-60s |  | - | 1.3 | 1.7 | 3.5 | 7.5 | 0.3 | - | 26.7 | 9.4 | 0.9 | 47.5 | 1.3 | - |
| C- 300s |  | - | 1.1 | 1.8 | 2.7 | 5.2 | 0.3 | - | 16.2 | 2.0 | 1.1 | 69.0 | 0.8 | - |
| C- 60s |  | 0.9 | 1.3 | 1.4 | 3.7 | 8 | 0.2 | - | 25.4 | 10 | 1 | 46.9 | 1.2 | - |

Table 3. Pore data estimated from image analysis of SEM micrographs.

| Specimen | Pore population density, mm-2 | Average pore size, µm | Porosity, % |
| --- | --- | --- | --- |
| AM-60s | 1.32×106 | 0.8 | 9.7 |
| AM-300s | 0.29×106 | 3.4 | 14.1 |
| C-60s | 0.90×106 | 1.1 | 13.1 |
| C-300s | 0.56×106 | 2.8 | 19.8 |

Table 4. Local EDS analysis (at.%) of cross sections of conventional (C) and DMLS (AM) substrates with flash-PEO (60s) and PEO (300s) coatings, as per locations in Figure 4.

| Specimen/ Location |  |  | Na | Mg | Al | Si | P | S | K | Ti | Ca | Zn | O | V | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AM-300s | Cross-sections | 1 | - | - | 2.5 | 0.2 | 0.3 | - | - | 22.8 | 0.1 | 0.1 | 71.6 | - | - |
|  |  | 2 | 0.7 | 0.4 | 1.6 | 2.5 | 5.5 | 1.3 | 0.3 | 17.9 | 2.1 | 0.2 | 66.8 | 0.7 | - |
|  |  | 3 | 0.5 | 0.6 | 2.1 | 2.4 | 4.2 | - | - | 14.0 | 2.7 | 0.2 | 0.5 | - | - |
| AM-60s |  | 1 | 0.3 | 0.4 | 2.6 | 1.3 | 2.9 | 0.7 | - | 19.9 | 1.3 | 0.7 | 69.8 | 0.7 | - |
|  |  | 2 | 0.2 | 1.2 | 1.8 | 1.8 | 5.2 | 0.2 | - | 11.2 | 4.4 | 3.3 | 72.8 | 0.4 | - |
| C-300s |  | 1 | 1.4 | - | 2.5 | 0.3 | 0.8 | 2.6 | 0.1 | 27.7 | - | - | 62.0 | 2.6 | - |
|  |  | 2 | 1.1 | 0.4 | 1.3 | 1.6 | 4.8 | 1.4 | 0.2 | 17.2 | 0.9 | 0.4 | 68.5 | 2.1 | - |
|  |  | 3 | - | 1.3 | 1.4 | 3.6 | 4.7 | 0.2 | - | 11.4 | 1.8 | 0.8 | 73.5 | 1.4 | - |
| C-60s |  | 1 | 0.4 | - | 2.8 | 1.0 | 3.4 | 1.5 | - | 22.5 | 0.4 | 0.1 | 67.3 | 0.6 | - |
|  |  | 2 | 0.6 | 1.5 | 1.4 | 3.5 | 5.8 | - | - | 11.0 | 7.3 | 0.2 | 68.0 | 0.7 | - |

Table 5. Corrosion and passive current densities following 1 h of immersion in SBF.

| Specimen | Ecorr (VAg/AgCl) | icorr (µA/cm2) | ipass (µA/cm2) |
| --- | --- | --- | --- |
| AM- Sub | -0.185 | 0.05 | 2.0 |
| C- Sub | -0.244 | 0.17 | 3.8 |
| AM-PEO 60s | 0.130 | 0.16 | 0.66 |
| AM-PEO 300s | 0.258 | 0.09 | 0.47 |
| C- PEO 60s | 0.268 | 0.19 | 0.47 |
| C- PEO 300s | 0.221 | 0.08 | 0.094 |

Table 6. Local EDS analysis (at.%) of conventional (C) and DMLS (AM) substrates with flash-PEO (60s) and PEO (300s) coatings, after 30 days immersion in SBF as per Figures 13, 14.

| Specimen/ Location |  | Na | Mg | Al | Si | P | K | Ti | Ca | Zn | O | V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C-sub | 1 | - | - | 7.7 | - | - | - | 70.9 | - | - | 18.6 | 2.8 |
| AM-sub | 1 | - | - | 8.8 | - | - | - | 71.1 | - | - | 17.9 | 2.2 |
|  | 2 | - | - | 9.9 | - | - | - | 75.4 | - | - | 12.1 | 2.7 |
| AM-300 s | 1 | 1.9 | 0.9 | 1.2 | 5.3 | 8.5 | - | 16.1 | 9.0 | 0.6 | 55.9 | 0.8 |
|  | 2 | - | 0.7 | 1.7 | 4.0 | 6.3 | - | 17.2 | 5.4 | 0.5 | 63.5 | 0.7 |
| C-300 s | 1 | - | 1.1 | 1.5 | 3.5 | 6.5 | - | 16.5 | 6.5 | 0.4 | 63.5 | 0.5 |
|  | 2 | - | 1.1 | 1.3 | 3.4 | 5.7 | 0.2 | 17.6 | 6.5 | 0.5 | 62.9 | 0.7 |
| AM-60 s | Plan view area | - | 1.4 | 1.1 | 3.2 | 6.6 | - | 11.1 | 6.5 | 0.4 | 69.2 | 0.5 |
| C-60 s |  | 0.7 | 1.1 | 1.2 | 2.9 | 5.7 | - | 13.2 | 5.5 | 0.4 | 68.6 | 0.7 |

Table 7. Roughness parameters and water contact angle before and after 30 days of immersion in SBF and corrosion testing.

| Sample |  | WCA, o | Sa, μm | S10z, μm |
| --- | --- | --- | --- | --- |
| AM-Sub | before | 73.9 | 0.12±0.01 | 1.0±0.1 |
|  | after | 67.7 | 0.63±.04 | 4.9±1.1 |
| C-Sub | before | 61.8 | 1.47±0.11 | 11.1±1.3 |
|  | after | 49.9 | 0.2±0.03 | 5.0±2.3 |
| AM-60s | before | 57.3 | 0.32±.02 | 4.7±1.7 |
|  | after | 62.4 | 1.2±0.4 | 9.7±5.4 |
| AM-300s | before | 58.3 | 0.53±.04 | 6.5±3.8 |
|  | after | 49.1 | 1.3±0.36 | 11.7±5.2 |
| C-60s | before | 61.8 | 0.35±.03 | 3.8±0.5 |
|  | after | 68.4 | 0.54±0.2 | 4.5±0.8 |
| C-300s | before | 62.5 | 0.55±.04 | 5.1±0.7 |
|  | after | 64.8 | 1.32±0.52 | 9.7±3.8 |

Table 8. Comparison of the PDP, ICP-OES and EIS derived values for oxidized Ti, Ti4+ lost into the SBF and barrier TiO2 thickness over 30 days of immersion in SBF.

| Specimen | Oxidized Ti, μg cm-2 | Ti4+in SBF, μg cm-2 | Ti4+ incorporated into the passive film, μg cm-2 | TiO2 thickness gain, nm | TiO2 thickness from EIS, nm |
| --- | --- | --- | --- | --- | --- |
| C-SUB | 54.65 | 0.88 | 53.77 | 2.34 | 2 |
| AM-SUB | 16.07 | 0.35 | 15.72 | 0.68 | 0.7 |
| C-300s | 25.72 | 2.67 | 23.05 | 1.00 | - |
| C-60s | 61.08 | 0.50 | 60.58 | 2.63 | - |
| AM-300s | 28.93 | 0.51 | 28.42 | 1.23 | - |
| AM-60s | 51.43 | 0.36 | 51.07 | 2.22 | - |