Table 1. Crystallinity percentage for Flash-PEO coatings calculated using XRD analysis software.

| Sample | Crystalline Fraction [%] | Amorphous Fraction [%] |
| --- | --- | --- |
| ACC | 87 | 13 |
| SiF | 85 | 15 |
| ACC-SiF | 80 | 20 |

Table 2. EDS results (at. %) for the studied coatings at locations labelled in Figure 6.

| ELEMENT | ACC |  |  | SiF |  |  | ACC-SiF |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | S1 | S2 | S3 | S1 Top | S2 Interm. | S3 Barrier | S1 Top | S2 Interm. | S3 Interm. | S4 Barrier |
| O | 49.3 | 32.5 | 51.6 | 55.2 | 51.6 | 31.8 | 54.3 | 51.3 | 44.5 | 21.4 |
| F | 21.0 | 33.2 | 22.7 | 1.4 | 4.0 | 12.5 | 5.3 | 6.8 | 9.0 | 9.3 |
| Na | - | - | - | 0.4 | 0.5 | - | 1.7 | 0.5 | - | - |
| Mg | 7.7 | 20.5 | 10.5 | 28.2 | 30.6 | 49.6 | 7.9 | 28.8 | 33.7 | 63.9 |
| Al | - | 0.9 | 0.9 | 1.7 | 1.3 | 1.9 | 0.7 | 1.3 | 1.2 | 2.5 |
| Si | - | - | - | 13.0 | 11.6 | 3.7 | 4.9 | 8.4 | 11.3 | 1.7 |
| K | 0.7 | 0.5 | 0.2 | - | - | - | 0.3 | - | - | - |
| Mn | 14.6 | 5.6 | 6.7 | 0.1 | 0.2 | 0.2 | 20.5 | 0.9 | 0.3 | 0.5 |
| Zn | - | - | 0.3 | - | 0.2 | 0.3 | 0.4 | - | - | 0.7 |
| Zr | 6.7 | 6.8 | 7.1 | - | - | - | 4.0 | 2.0 | - | - |

Table 3. Elemental composition based on XPS survey of the samples: as-received (a-r) and after 10 min sputtering* cleaning (s-c).

|  | O | F | Mg | Si | Mn | Zr | K |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ACCa-r | 42.9 | 17.1 | 5.4 | - | 9.6 | 8.0 | - |
| SiFa-r | 56.0 | 2.2 | 16.2 | 12.7 | 0.1 | - | - |
| ACC-SiFa-r | 58.6 | 1.9 | 15.9 | 13.8 | 1.8 | 0.4 | - |
| ACCs-c | 46.6 | 14.2 | 5.4 | - | 17.3 | 12.2 | 0.3 |
| SiFs-c | 51.6 | 2.0 | 31.3 | 13.2 | 0.2 | - | - |
| ACC-SiFs-c | 54.0 | 1.7 | 24.5 | 12.5 | 3.5 | 2.6 | - |

* Sputtering removes approximately 460 nm of the outer part of the coating.

Table 4. Main compounds present in ACC-SiF coating. XRD and XPS data correlation.

| Compound | XRD peaks (°2θ) | XPS peaks |
| --- | --- | --- |
| ZrO2 | 30.2, 35.2, 50.4 | Zr3d at ~182.0 eV and Zr4s at 53.1 eV |
| MnO | 41.1 | Mn2p satellite in Mn2p |
| MnO2 | - | Mn2p asymmetry at 641.6 eV |
| MgO | 42.9 | Mg2p at ~50.5 eV |
| MgF2 | - | F1s at 685.3 eV, Mg2p at 50.7 eV |
| MgSiO3 | - | Mg2p at ~50.7 eV, Si2p at ~101.9 eV, O1s ~531.0 eV |
| SiO2 | - | Si2p peak at ~103.0 eV |

Table 5. EIS parameters after immersion to 0.5 wt.% NaCl obtained by fitting the impedance plots, using equivalent electrical circuits.

| System | χ2 |  |  |  | CPEdl [Ω-1·cm-2 ·sα] | αdl | Rct [Ω·cm2] | Cappdl [F·cm-2] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AZ31B 24h | (4.7±2.1)10-3 |  |  |  | (2.5±0.8)10-5 | 0.85±0.02 | (4.5±3.4)103 | (1.7±0.7)10-5 |
| AZ31B 48h | (8.9±1.0)10-4 |  |  |  | (3.4±1.3)10-5 | 0.82±0.03 | (4.6±2.7)103 | (2.3±1.1)10-5 |
| AZ31B 168h | (1.1±0.4)10-3 |  |  |  | (3.3±0.2)10-5 | 0.80±0.01 | (1.8±0.2)103 | (1.7±0.1)10-5 |
| ACC 24h | (1.1±0.1)10-3 |  |  |  | (2.1±0.2)10-5 | 0.88±0.01 | (1.1±0.0)103 | (1.2±0.1)10-5 |
| ACC 48h | (6.4±3.2)10-4 |  |  |  | (2.5±0.4)10-5 | 0.82±0.02 | (1.1±0.2)103 | (1.1±0.2)10-5 |
| ACC 168h | (3.4±0.5)10-4 |  |  |  | (1.9±0.5)10-5 | 0.82±0.03 | (1.5±0.2)103 | (8.9±3.0)10-6 |
| System | χ2 | CPEout [Ω-1·cm-2·sα] | αout | Rout [Ω·cm2] | CPEin [Ω-1·cm-2 ·sα] | αin | Rin [Ω·cm2] | Cappin / Cappdl [F·cm-2] |
| SiF 24h | (4.8±1.6)10-3 | (1.4±0.2)10-7 | 0.85±0.01 | (7.7±4.2)104 | (7.8±2.1)10-8 | 0.99±0.01 | (5.7±0.5)107 | (8.0±2.1)10-8 |
| SiF 48h | (8.7±4.5)10-4 | (2.2±0.3)10-7 | 0.87±0.02 | (8.5±4.0)104 | (6.8±2.0)10-8 | 0.97±0.03 | (5.0±2.9)106 | (6.6±2.0)10-8 |
| SiF 168h | (1.7±1.3)10-4 | (1.8±0.3)10-6 | 0.95±0.00 | (2.2±0.8)105 | (2.8±1.1)10-5 | 0.69±0.17 | (1.4±0.9)105 | (5.1±4.3)10-5 |
| ACC-SiF 24h | (5.9±2.9)10-3 | (1.3±0.0)10-7 | 0.86±0.01 | (3.4±0.5)104 | (7.2±1.1)10-8 | 0.95±0.01 | (1.5±1.1)109 | (9.2±1.6)10-8 |
| ACC-SiF 48h | (2.7±0.7)10-3 | (1.3±0.3)10-7 | 0.88±0.03 | (3.1±1.1)104 | (7.5±3.0)10-8 | 0.94±0.04 | (3.3±1.7)108 | (9.1±4.1)10-8 |
| ACC-SiF 168h | (1.3±6.1)10-4 | (2.3±0.5)10-6 | 0.95±0.00 | (8.9±2.4)104 | (7.2±2.1)10-5 | 0.66±0.12 | (4.5±1.5)104 | (1.3±0.7)10-4 |

Table 6. PDP averaged values for -ϐc, icorr, Ecorr and Pcorr for 1-, 12- and 24-hours testing.

| 1 hour |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | -ϐc [V·dec-1] | icorr [A·cm-2] | Ecorr vs. Ag/AgCl [V] | Pcorr [mm·yr-1] |
| AZ31B | 0.17±0.01 | (1.15±0.57)10-6 | -1.20±0.06 | (2.63 ±1.3)10-2 |
| ACC | 0.14±0.02 | (3.51±0.95)10-6 | -1.29±0.01 | (8.00±2.18)10-2 |
| SiF | 0.19±0.01 | (3.91±3.65)10-8 | -1.38±0.01 | (8.92±8.34)10-4 |
| ACC-SiF | 0.20±0.02 | (6.60±1.83)10-9 | -1.05±0.02 | (1.51±0.41)10-4 |
| 12 hours |  |  |  |  |
| AZ31B | 0.15±0.00 | (4.38±0.17)10-6 | -1.27±0.01 | (9.99±0.36)10-2 |
| ACC | 0.13±0.01 | (1.23±0.17)10-6 | -1.23±0.00 | (2.81±0.40)10-2 |
| SiF | 0.18±0.01 | (1.42±1.05)10-9 | -1.10±0.02 | (3.25±2.39)10-5 |
| ACC-SiF | 0.23±0.06 | (2.27±0.87)10-10 | -0.84±0.08 | (5.18±2.00)10-6 |
| 24 hours |  |  |  |  |
| AZ31B | 0.16±0.00 | (2.60±0.71)10-6 | -1.25±0.02 | (5.93±1.63)10-2 |
| ACC | 0.12±0.00 | (7.33±2.62)10-7 | -1.21±0.02 | (1.67±0.59)10-2 |
| SiF | 0.18±0.05 | (5.87±3.67)10-10 | -1.10±0.03 | (1.34±0.83)10-5 |
| ACC-SiF | 0.35±0.0 | (1.51±0.45)10-10 | -0.64±0.07 | (3.45±1.04)10-6 |

Table 7. Averaged Modulus of Impedance (|Z|0.01 Hz) at 10 mHz for Flash-PEO coated specimens without and with pre-existing defect.

|  | ¦Z¦0.01 Hz SiF (Ω·cm2) | ¦Z¦0.01 Hz SiF Defect (Ω·cm2) | ¦Z¦0.01 Hz ACC-SiF (Ω·cm2) | ¦Z¦0.01 Hz ACC-SiF Defect (Ω·cm2) |
| --- | --- | --- | --- | --- |
| 24 h | (3.5±0.3)107 | (2.7±1.7)107 | (6.0±0.6)107 | (3.9±2.9)107 |
| 48 h | (5.4±2.8)106 | (1.2±0.8)107 | (4.6±1.6)107 | (3.5±2.0)107 |
| 72 h | (2.6±1.0)106 | (3.1±0.9)106 | (1.4±1.0)107 | (7.0±7.7)106 |
| 96 h | (1.6±0.7)105 | (1.1±0.4)106 | (2.5±1.7)106 | (1.1±0.7)106 |
| 120 h | (1.1±6.0)105 | (3.5±0.6)105 | (5.4±4.0)105 | (3.0±2.7)105 |
| 144 h | (5.6±2.5)105 | (1.9±0.9)105 | (2.4±1.8)105 | (8.4±14.0)104 |
| 168 h | (3.1±1.2)105 | (1.3±0.4)105 | (1.3±0.9)105 | (5.6±9.2)104 |