## Slide 1
Permanganate-fluorozirconate conversion coating as precursor for Flash-
PEO on AZ31B magnesium alloy
Imágenes consolidadas artículo

## Slide 2
Graphical Abstract

## Slide 3
Alkaline Bath
pH 12.8
~85 ºC
15 min
Acid Bath
pH 1.1
~20 ºC
4 min
ACC Bath
pH 2.1
~45 ºC
30 min
Flash-PEO
pH ~ 12.8 | ~ 25 mS·cm-1
~20 ºC
350 VDC | 100 mA·cm-2
60 s
CLEANING
CONVERSION
ACC
ACC-SiF
Figure 1. Flow diagram of the implemented surface treatment process for AZ31B Mg alloy samples, showing the characteristic resultant ACC precursor and ACC-SiF structured coating sample after Flash-PEO processing.

## Slide 4
St1
St2
St3
V
i
V
i
SiF Energy Consumption
0.55 [kWh·m-2·µm-1]
ACC-SiF Energy Consumption
0.47 [kWh·m-2·µm-1]
a
b
Figure 2. Voltage - Current characteristic profile for SiF and ACC-SiF coatings formation during Flash-PEO processing, b) Initial evolution of electrical parameters of the process.

## Slide 5
Figure 3. (a-f) Still video frames of Flash-PEO SiF processing: a) 0 s; b) 1 s; c) 2 s, continuous evolution of oxygen with bubble size slightly increasing; d) 10 s, first microdischarges at 250 V; e) 30 s, microdischarges at 350 V before current density drops, end of St1 and beginning of St2; f) 60 s, finalization of St3. (g-l) Still video frames of Flash-PEO ACC-SiF processing: g) 0 s; h) 1 s; i) 2 s continuous evolution of oxygen with bubble size increasing; j) 12 s, first microdischarges, noticed visually at 210 V; k) 30 s, microdischarges at 350 V before current density drop, end of St1 and beginning of St2; l) 60 s, finalization of St3. (Supplementary Information, Video S1 and S2).

## Slide 6
Figure 4. XRD spectrum for, a) AZ31B reference sample; b) ACC conversion coating; c) SiF coating and d) ACC-SiF coating.

## Slide 7
Figure 5. SEM-BSE plain view images and EDS analysis results in atomic percentage (in-set) of the AZ31B Mg alloy surface samples with the processed coatings. Red square shows the area of interest magnified. a) and b) ACC conversion coating; c) and d) SiF coating; e) and f) ACC-SiF coating.

## Slide 8
Figure 6. Cross section SEM-BSE images of the AZ31B Mg alloy surface samples with the processed coatings a) and b) ACC conversion coating; c) and d) SiF coating; e) and f) ACC-SiF coating. Red square shows the area of interest magnified and with indications of EDS spot locations shown in Table 2.

## Slide 9
Figure 7. High resolution XPS spectra for (a-c) C1s and K2p, (d-f) F1s, (g-i) Mg2p, (j, k) Si2p, (l, m) Zr3d and (n-p) O1s for ACC conversion coating, SiF coating and ACC-SiF coating, as indicated.

## Slide 10
Figure 8. High resolution XPS spectrum for Mn2p: a) ACC conversion coating; b) SiF coating; c) ACC-SiF coating; d) Mn 2p3/2 and to Mn2p1/2 states and satellite indication, and e) Asymmetry at 641.6 eV in ACC and ACC-SiF.

## Slide 11
Figure 9. a) Open Circuit Potential (OCP) record for 7 days immersion in 0.5 wt.% NaCl solution for specimens under study and b) EIS values at |Z|0.01 Hz Bode Plot versus immersion time for all the samples.

## Slide 12
Figure 10. Bode plots for the module of impedance (|Z|) versus frequency and Nyquist plots for bare and coated AZ31B Mg alloy after a, d) 24 h, b, e) 48 h and c, f) 168 h immersion in 0.5 wt.% NaCl respectively. Continuous lines correspond to the fitted data.

## Slide 13
Figure 11. Polarization curves after 1-, 12- and 24-hours of immersion in 0.5 wt.% NaCl for a) AZ31B reference sample; b) ACC conversion coating; c) SiF coating and d) ACC-SiF coating.

## Slide 14
Figure 12. OM images of SiF coating sample with pre-existing defect a) before; c) after immersion in 0.5 wt.% NaCl solution. OM images for ACC-SiF coating with pre-existing defect b) before and d) after EIS. Indication of damage mechanisms observed in SiF OM image c) and ACC-SiF d) (SEM image inset). Consolidated EIS results representing in Bode Plot, the logarithm of the impedance modulus |Z| at 0.01 Hz for Flash-PEO coated samples (SiF coating / ACC-SiF coating) with pre-existing defect.