## Slide 1
Permanganate-fluorozirconate conversion coating as precursor for Flash-
PEO on AZ31B magnesium alloy
Imágenes suplementarias consolidadas artículo

## Slide 2
Figure S1. Surface characterization of the produced coatings. a) Appearance of ACC conversion coating, contact angle and surface roughness; b) Appearance of SiF coating, contact angle and surface roughness and c) Appearance of ACC-SiF coating, contact angle and surface roughness. Porosity analysis for, d) SiF coating and e) ACC-SiF coating.

## Slide 3
Figure S2. Hardness characterization by using micro indenter device for uncoated and coated Flash-PEO samples.

## Slide 4
ACC-SiF
SiF
~ 0.4 µm
Substrate
top layer
barrier layer
~ 0.4 µm
intermediate layer
Substrate
top layer
barrier layer
intermediate layer
a
b
Figure S3. TEM images for a) SiF and b) ACC-SiF coating.

## Slide 5
Figure S4. XPS survey spectra of the coated samples under study, showing the C1s reference signal at 284.8 eV for a) as-received (a-r) and b) after 10 min of argon sputtering (s-c).

## Slide 6
Figure S5. Equivalent electrical circuits used to fit EIS data. Model EC-1 (a) and Model EC-2 (b).

## Slide 7
Figure S6. Impedance curves for SiF samples at 24-, 48- and 168-hours immersion in in 0.5 wt.% NaCl.

## Slide 8
Figure S7. Impedance curves for ACC-SiF samples at 24-, 48- and 168-hours immersion in 0.5 wt.% NaCl.

## Slide 9
Figure S8. Polarization curves for independent SiF samples after 1-, 12- and 24-hours immersion in 0.5 wt.% NaCl.

## Slide 10
Figure S9. Polarization curves for independent ACC-SiF samples after 1-, 12- and 24-hours immersion in 0.5 wt.% NaCl.

## Slide 11
Figure S10. SEM BSE micrographs for SiF coating with defect (a, b) and for ACC-SiF coating with defect (c, d), after 168 h immersion in 0.5 wt.% NaCl solution. SEM-SE plain view images and EDS analysis results in at.% (in-set) of the coatings with pre-existing defect after 168 h of EIS (e) SiF; (f) ACC-SiF.