Table 1. Dip-coating conditions for the fabrication of polymeric layers of HHC.

| Coating layer | Withdrawal speed | No. of immersion cycles |
| --- | --- | --- |
| Sealing PCL | 0.3 mm/s | 1 |
| BF PCL | 2 mm/s | 2 |