Figure 1. Potentiodynamic polarization curves of AA2024 alloy after (a) 1 hour and (b) 24 hours of immersion in naturally aerated 50 mM NaCl solutions with different TA concentrations.

Figure 2. (a,b) Topography and (c,d) Volta potential maps for AA2024 before and after immersion for 1 hour in blank solution (50 mM NaCl). (e,f) Topography and (g,h) Volta potential maps for AA2024 before and after immersion for 1 hour in 1 mM TA solution.

Figure 3. Surface images and SVET maps of AA2024-T3 immersed in 50 mM NaCl (a-c) and 1 mM TA solutions (d-f). The maps were acquired after 1 hour (a, d), 6 hours (b, e), and 24 hours (c, f) of immersion. The current density units depicted in the maps are µA cm-2.

Figure 4. (a) UV-Vis absorption spectra of Tannic acid, Cu, and Al chloride solutions and corresponding mixing solutions. Equimolar mixtures of tannic acid with CuCl2 solution: (b) 10 µM, (c) 1 mM, and (d) 10 mM; and equimolar mixtures of tannic acid with AlCl3 solutions: (e) 10 µM, (f) 1 mM, and (g) 10 mM.

Figure 5. Bode plots of AA2024 alloy after different immersion times in naturally aerated (a) 50 mM NaCl solutions with different TA concentrations: (b) 0.1 mM TA, (c) 1 mM TA, and (d) 10 mM TA.

Figure 6. Equivalent circuits to fit the experimental EIS data of the AA2024 in naturally aerated (a) 50 mM NaCl solution and (b) TA-containing solutions.

Figure 7. Evolution of (a) oxide capacitance, (b) charge transfer resistance, and (c) double-layer capacitance of the AA2024 alloy during the studied immersion times in the study solutions.

Figure 8. (a) Macroscopic, and (b) detailed view of the AA2024 samples after 7 days of immersion in naturally aerated 50 mM NaCl solutions with different TA concentrations.

Figure 9. Scanning electron micrographs of the AA2024 samples after 7 days of immersion in naturally aerated 50 mM NaCl solutions: (a,b) blank; (c-e) 0.1 mM; (f-h) 1 mM; and 10 mM (i-k) TA solutions.

Figure 10. (a) Raman analysis and (b) water contact angle of the AA2024 samples after 7 days of immersion in naturally aerated 50 mM NaCl (blank) and TA-based solutions.

Figure 11. 3D topographical maps of AA2024 surface after 7 days of immersion in naturally aerated 50 mM NaCl (blank) and TA-based solutions.

Figure 12. Schematic illustration for inhibition mechanism of tannic acid for the AA2024 alloy.