Data for the paper entitled, “Corrosion inhibitor from nature: Fundamentals of tannic acid inhibition for AA2024 alloy” including:

- Processed Data: Raman spectra, roughness, polarization and electrochemical impedance spectroscopy curves on AA2024-T3 after immersion in different tannic acid-containing solutions.

- Processed Images: Optical microscopy, scanning electron micrographs, scanning kelvin probe force microscopy, scanning vibrating electrode technique, and optical profilometry images of AA2024-T3 alloy after immersion in different tannic acid-containing solutions.

- Tables (processed data)