Table 1. Summary of the most efficient corrosion inhibitors for AA2024 alloy.

| Inhibitor | Time (h) | pH/Temperature (K) | Inhibitor/NaCl concentration (mM) | Efficiency (%) | Acute Toxicity LD50 Oral rat (mg/Kg)/ Carcinogenicity Toxicity fish,mg/L | References |
| --- | --- | --- | --- | --- | --- | --- |
| Benzotriazol derivates (2- mercaptobenzothiazole (2-MBT), 2-mercaptoacetic acid, 4-mercaptobenzoic acid, benzotriazole, etc) | 24-672 | 7/298 | (5-50)/100 | 87-95 | Equivocal tumorigenic agent (560)/ Harmful to aquatic life with long-lasting effects (25) | [10, 14] |
| 8-HQ | 24 | 7 | (3-50)/50 | 72-84 | (n/a)/ Potentially mutagenic (18) | [9, 15] |
| Cerium-based salts (Ce(NO3), (NH4)2Ce(NO3)5, Ce2(SO4)3, CeCl3) | 144-600 | 7/298 | 1/10 | 96-97.5 | Not identified (4200)/ Very toxic to aquatic life with long-lasting effects (0.3) | [11] |
| Ferrous and zinc gluconate | 48-192 | 7/301 | (10-42)/50 | 99 | Very toxic to aquatic life (n/a) | [12, 16] |
| Vanadate-based salts (NH4VO3, NaVO3) | 1 | 3-10/298 | (3.2-320)/100 | - | Very toxic to aquatic life (n/a) | [6, 17, 18] |
| Lithium carbonate | 24 | -/298 | 5/50 | 76 | Known or potential hazard for reproductive toxicity (n/a) | [10] |
| + Notes: 1 - The inhibitor efficiency is usually calculated by potentiodynamic polarization (PDP), electrochemical impedance spectroscopy (EIS), and/or mass loss after the immersion test. 2 - The toxicity data were reported in [6, 19]. |  |  |  |  |  |  |

Table 2. The corrosion potential, current densities, and inhibition efficiency of tannic acid on the AA2024 alloy after 1 and 24 hours of immersion in naturally aerated 50 mM NaCl solutions with different TA concentrations.

| Solution | icorr (A cm-2) |  | Ecorr (mV) vs SCE | Ebreakdown (mV) vs SCE | IE (%) |
| --- | --- | --- | --- | --- | --- |
|  |  | 1 hour of immersion |  |  |  |
| Blank | (3.20 ± 3.00) ·10-7 |  | -541.0 ± 10.0 | -538.0 ± 8.0 | - |
| 0.1 mM TA | (6.70 ± 1.70) ·10-6 |  | -515.0 ± 30.0 | -510.5 ± 20.0 | -110 |
| 1 mM TA | (1.60 ± 0.20) ·10-7 |  | -478.0 ± 7.0 | -468.0 ± 10.0 | 51 |
| 10 mM TA | (1.70 ± 0.50) ·10-8 |  | -482.5 ± 1.0 | -475.0 ± 3.0 | 94 |
|  |  | 24 hours of immersion |  |  |  |
| Blank | (2.60 ± 0.50) ·10-6 |  | -762.5 ± 12.0 | -512.3 ± 8.0 | - |
| 0.1 mM TA | (2.50 ± 3.00) ·10-6 |  | -594.0 ± 37.8 | -489.3 ± 27.0 | 4 |
| 1 mM TA | (1.20 ± 0.20) ·10-6 |  | -533.0 ± 2.0 | -438.2 ± 4.4 | 55 |
| 10 mM TA | (2.20 ± 0.10) ·10-7 |  | -588.0 ± 38.0 | -592.4 ± 28.5 | 87 |

Table 3. Fitted electrical parameters of the AA2024 after the tested immersion times in naturally aerated 50 mM NaCl solutions with different TA concentrations.

| Solution | Immersion time [days] | Rsol [Ω cm2] | R-ox [KΩ cm2] | CPE-ox [F sn-1 cm-2] | nox | R-ct [KΩ cm2] | CPE-dl [F sn-1 cm-2] | ndl | W [mS s1/2 cm-2] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Blank | 1 hour | 9.2 | 1.3 | 2.0·10-4 | 0.9 | 3.1 | 1.1·10-4 | 0.6 | 0.8 |
|  | 1 | 31.9 | - | - | - | 11.9 | 5.5·10-4 | 0.7 | 5.4 |
|  | 2 | 26.6 | - | - | - | 4.5 | 5.3·10-4 | 0.6 | 28.0 |
|  | 4 | 23.9 | - | - | - | 1.7 | 3.1·10-3 | 0.9 | 1.0 |
|  | 7 | 29.7 | - | - | - | 1.0 | 2.1·10-3 | 0.9 | 0.9 |
| 0.1 mM TA | 1 hour | 7.7 | 138.8 | 2.7·10-5 | 0.9 | 428.0 | 9.4·10-6 | 0.9 | - |
|  | 1 | 15.7 | 111.1 | 3.5·10-5 | 0.9 | 376.4 | 2.1·10-6 | 0.9 | - |
|  | 2 | 24.2 | 57.3 | 6.7·10-5 | 0.9 | 252.7 | 3.9·10-6 | 0.9 | - |
|  | 4 | 4.2 | 75.5 | 7.2·10-5 | 0.9 | 300.0 | 1.6·10-6 | 0.8 | - |
|  | 7 | 39.7 | 96.2 | 2.1·10-4 | 0.8 | 210.3 | 2.4·10-5 | 0.9 | - |
| 1 mM TA | 1 hour | 31.0 | 455.5 | 6.0·10-5 | 0.9 | 588.7 | 6.2·10-5 | 0.8 | - |
|  | 1 | 9.3 | 40.9 | 1.9·10-5 | 0.9 | 415.1 | 2.2·10-5 | 0.9 | - |
|  | 2 | 11.5 | 54.8 | 1.0·10-4 | 0.8 | 234.8 | 9.1·10-5 | 0.8 | - |
|  | 4 | 16.5 | 88.5 | 1.1·10-4 | 0.8 | 260.3 | 2.8·10-5 | 0.7 | - |
|  | 7 | 46.2 | 74.4 | 2.4·10-4 | 0.8 | 250.0 | 4.7·10-5 | 0.7 | - |
| 10 mM TA | 1 hour | 22.55 | 37.9 | 1.0·10-5 | 0.9 | 919.4 | 2.5·10-5 | 0.7 | - |
|  | 1 | 21.8 | 27.7 | 2.6·10-5 | 0.9 | 178.5 | 9.2·10-5 | 0.8 | - |
|  | 2 | 8.3 | 26.5 | 1.4·10-5 | 0.9 | 215.0 | 3.0·10-4 | 0.8 | - |
|  | 4 | 18.4 | 16.0 | 2.1·10-4 | 0.8 | 172.5 | 8.4·10-4 | 0.9 | - |
|  | 7 | 25.0 | 8.1 | 2.8·10-4 | 0.8 | 18.3 | 7.0·10-4 | 0.9 | - |

Table 4. EDS analysis (at.%) of the AA2024 samples after 7 days of immersion in naturally aerated 50 mM NaCl (blank) and TA-based solutions. Matrix analysis have been performed at lower magnifications. Deposit locations are denoted on SEM images in Figure 9.

| Solution | Zone | C | O | Mg | Al | Cu |
| --- | --- | --- | --- | --- | --- | --- |
| Blank | Matrix | 17.2 | 49.4 | 0.4 | 32.3 | 0.7 |
|  | Deposit | 18.3 | 50.1 | 0.4 | 30.6 | 0.6 |
| 0.1 mM | Matrix | 32.6 | 2.4 | 1.1 | 62.9 | 0.9 |
|  | Deposit | 49.8 | 6.9 | 0.8 | 41.9 | 0.7 |
| 1 mM | Matrix | 49.4 | 4.9 | 0.8 | 44.4 | 0.6 |
|  | Deposit | 45.7 | 20.9 | 0.7 | 32.6 | 0.1 |
| 10 mM | Matrix | 47.4 | 9.9 | 0.8 | 41.3 | 0.6 |
|  | Deposit | 46.7 | 21.9 | 0.6 | 30.4 | 0.4 |