## Slide 1
Growth behavior of energy-efficient protective black flash-PEO coatings on additively manufactured aluminum‒silicon alloys
Muhammad Ahsan Iqbal*, Endzhe Matykina, Itziar Hidalgo-González, Raul Arrabal, Marta Mohedano
Departamento de Ingeniería Química y de Materiales, Facultad de Ciencias Químicas, Universidad Complutense de Madrid, 28040 Madrid, Spain

## Slide 2
Figure 1. (a) The variation in the voltage with time during the PEO process, (b) ΔE0 value of the PEO, and macroscopic images of developed PEO coatings, (c) PEO-2, (d) PEO-3, (e) PEO-4, (f) PEO-5.

## Slide 3
Figure 2. Dimensional representation of the CIE Lab color model: (a) General diagram of the color model, (b) CIE Lab color model of the PEO-4 specimen

## Slide 4
Figure 3. SEM top views of the developed coatings and EDS spectra: (a, b) PEO-2, (c, d) PEO-3, (e, f) PEO-4, and (g, h) PEO-5.

## Slide 5
Figure 4. Cross-sectional images of the developed PEO films: (a) PEO-2, (b) PEO-3, (c) PEO-4, and (d) PEO-5.

## Slide 6
Figure 5. SEM and EDS mapping images of developed PEO coatings elements.

## Slide 7
Figure 6. Surface roughness, (a) PEO-2, (b) PEO-3, (c) PEO-4, (d) PEO-5.

## Slide 8
Figure 7. X-ray diffraction patterns of the developed black PEO coatings.

## Slide 9
Figure 8. Raman spectra of the developed PEO coatings: (a) PEO-2, (b) PEO-3, (c) PEO-4, and (d) PEO-5.

## Slide 10
Figure 9. Vicker hardness values of the bare substrate and PEO-treated substrate after different durations.

## Slide 11
Figure 10. EIS spectra of the developed coatings for different immersion times, (a-c) after 1 day, and (d-f) after 10 days immersion in 3.5 wt.% NaCl solution.

## Slide 12
Figure 11. Equivalent circuits used for the developed PEO coatings: (a) immersion time of 24 h and (b) immersion time of 240 h.

## Slide 13
Figure 12. Macroscopic images of the PEO-treated samples after 10 days of immersion in 3.5 wt.% NaCl: (a) PEO-2, (b) PEO-3, (c) PEO-4, and (d) PEO-5; and CIE Lab color model of the PEO-4, (f) as-prepared, (g) after 10 days immersion in 3.5 wt.% NaCl.

## Slide 14
Figure 13. The color variation (∆E) values of the developed black flash-PEO samples before and after 10 days of immersion in a 3.5% NaCl solution.