Table 1. Black PEO coatings on aluminum base alloys under different conditions reported in the literature.

| Substrate | Electrolyte | Additive | Treatment Conditions | Coloring Analysis* | Corrosion resistance | Ref |
| --- | --- | --- | --- | --- | --- | --- |
| Al-12Si | (NaPO3)6, | NH4VO3 | 100 mA/cm2 ≥800 sec | As prepared: N/A Postcorrosion: N/A | N/A | [25] |
| 1060 Al | (NaPO3)6, NaOH | NH4VO3 , Na2WO4 | 20 min at 900 Hz frequency and 20% duty cycle with a constant current density of 150 mA/cm2. | As prepared: αs ≈90% Postcorrosion: N/A | N/A | [26] |
| Al-Si alloy | (NaPO3)6, NaOH | NH4VO3 , Na2WO4 | 100 to 400 V negative voltage was fixed at 30 V 1 kHz, and the duty ratio was 30%. All the samples were PEO treated for 14 min. | L=31.51, a=1.37, b=0.5 Post corrosion: N/A | N/A | [18] |
| 6061 Al | Na2SiO3 NaOH | VOSO4 | 50 Hz 10 A dm−2 10 min | As prepared: N/A, αs/εIR ratio ≈1.0 Post corrosion: N/A | N/A | [27] |
| 7075 Al | Na2SiO3 (NaPO3)6, NaOH | NH4VO3 | Constant voltage model of 460 V/−40 V, duty cycle 40 %/−20 % 100-600 Hz | As prepared: L=19, a=0, b=1 at 200 Hz Pos tcorrosion: N/A | ¦Z¦0.01 107 after 1 hr in 3.5 wt.% NaCl | [28] |
| 6061 Al | (NaPO3)6, KOH | NH4VO3 K2Cr2O7 | Constant current of 1.8 A/cm2 and a pulse frequency of 900 Hz upto 40 min | As prepared: αs ≈90% Pos tcorrosion: N/A | --- | [19] |
| 7075 Al | 3 g/L Na2SiO4·9H2O + 6 g/L KOH | (NH4)6Mo7O24, K2TiF6, Na2WO4·2H2O | 10 min at 1000 Hz frequency and 20% duty cycle under a constant current density of 150 mA/cm2 | As prepared: αs ≈90% Pos tcorrosion: N/A | icorr (μA/cm2) 10-4 to 10-5 in 3.5 wt.% NaCl | [17] |

*L-a-b (coloring parameters in color space model), αs - solar absorptance, εIR - infrared emittance

Table 2. Chemical composition of the Flash-PEO electrolyte.

| Electrolyte Composition | Conductivity (µS/cm) | PEO treatment (min) | Sample |
| --- | --- | --- | --- |
| (NaPO3)n 20 g/L, Na2EDTA·2H2O 28 g/L, NH4VO3 9 g/L, 1 g/L KOH | pH= 9.3 σ =12.9 ± 0.02 | 2 | PEO-2 |
|  |  | 3 | PEO-3 |
|  |  | 4 | PEO-4 |
|  |  | 5 | PEO-5 |

Table 3. Coating parameters obtained under certain conditions.

| Specimen |  | PEO thickness (μm) | Specific energy consumption, EPEO (kW.h.m−2.μm−1) |
| --- | --- | --- | --- |
| PEO-2 |  | 4.9±1.3 | 1.03 |
| PEO-3 |  | 5.1±1.1 | 1.47 |
| PEO-4 |  | 5.9±1.3 | 2.05 |
| PEO-5 |  | 5.8±1.2 | 2.20 |

Table 4. The elemental composition (at. %) of the developed coatings (Figures 3 and 4).

| PEO-2 | O | Al | P | V | Si |
| --- | --- | --- | --- | --- | --- |
| Surface (plan view) | 59.0 | 22.8 | 8.4 | 4.3 | 6.8 |
| Point 1 (outer region) | 55.2 | 23.0 | 7.2 | 3.3 | 5.8 |
| Point 2 (inner region) | 52.8 | 37.2 | 4.2 | 1.1 | 2.6 |
| PEO-3 | O | Al | P | V | Si |
| Surface (plan view) | 58.1 | 21.0 | 10.6 | 7.82 | 6.2 |
| Point 1 (outer region) | 55.7 | 28.6 | 9.43 | 6.65 | 5.6 |
| Point 2 (inner) | 39.7 | 44.7 | 4.58 | 3.20 | 3.2 |
| PEO-4 | O | Al | P | V | Si |
| Surface (plan view) | 55.5 | 20.3 | 11.4 | 9.53 | 6.0 |
| Point 1 (outer region) | 53.4 | 25.4 | 10.33 | 8.94 | 5.7 |
| Point 2 (inner region) | 47.6 | 36.8 | 5.73 | 3.52 | 3.8 |
| PEO-5 | O | Al | P | V | Si |
| Surface (plan view) | 54.0 | 20.4 | 12.7 | 9.3 | 6.0 |
| Point 1 (outer region) | 58.4 | 21.7 | 11.1 | 9.37 | 5.3 |
| Point 2 (inner region) | 58.6 | 27.1 | 5.61 | 3.54 | 3.2 |

Table 5. Evolution with time of the fitting parameters Rout, CPEout, αout, Rin, CPEin, αin Rct, Qdl, and αdl after 24 hr of immersion.

| Sample | CPEout Ω-1 cm-2 sα | αout | Rout Ω cm2 | CPEin Ω-1 cm-2 sα | αin |  | Rin Ω cm2 | CPEdl Ω-1 cm-2 sα | αdl | Rct Ω cm2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PEO-2 | 3.24×10-6 ±0.38×10-6 | 1.00 ±0.09 | 4.51×101 ±0.29 | 7.85×10-7 ±0.58×10-7 | 0.91 ±0.04 | 9.41×104 ±0.15 |  | 4.45×10-6 ±0.35×10-6 | 0.67 ±0.07 | 2.7×103 ±0.12 |  |
| PEO-3 | 1.63×10-8 ±0.28×10-8 | 0.74 ±0.08 | 6.51×101 ±0.37 | 2.09×10-7 ±0.49×10-7 | 0.89 ±0.04 | 7.75×104 ±0.26 |  | 6.49×10-5 ±0.39×10-5 | 0.96 ±0.07 | 1.0×105 ±0.11 |  |
| PEO-4 | 8.68×10-8 ±0.27×10-8 | 0.80 ±0.07 | 1.02×102 ±0.37 | 5.47×10-8 ±0.37×10-8 | 1.00 ±0.03 | 1.12×105 ±0.29 |  | 1.34×10-6 ±0.26×10-6 | 1.00 ±0.06 | 6.0×105 ±0.12 |  |
| PEO-5 | 2.85×10-7 ±0.29×10-7 | 1.00 ±0.07 | 5.90×101 ±0.46 | 1.68×10-6 ±0.35×10-6 | 1.00 ±0.03 | 8.99×104 ±0.18 |  | 1.24×10-6 ±0.24×10-6 | 0.88 ±0.07 | 8.7×104 ±0.30 |  |

Table 6. Evolution with time of the fitting parameters Rout, CPEout, αout, Rin, CPEin, αin Rct, Qdl, and αdl after 240 hr of immersion.

| Sample | CPEout Ω-1 cm-2 sα | αout | Rout Ω cm2 | CPEin Ω-1 cm-2 sα | αin | Rin Ω cm2 | CPEdl Ω-1 cm-2 sα | αdl | Rct Ω cm2 | w Ω-1 cm-2 s5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PEO-2 | 1.28×10-7 ±0.38×10-7 | 1.00 ±0.01 | 1.33×101 ±0.17 | 1.34×10-5 ±0.28×10-5 | 0.97 ±0.03 | 1.36×104 ±0.15 | 4.27×10-6 ±0.38×10-6 | 0.68 ±0.02 | 1.0×102 ±0.09 | 5.0×10-5 ±0.38×10-5 |
| PEO-3 | 1.49×10-7 ±0.21×10-7 | 1.00 ±0.02 | 8.47×101 ±0.21 | 1.74×10-5 ±0.30×10-5 | 0.87 ±0.04 | 1.48×104 ±0.19 | 9.23×10-6 ±0.28×10-6 | 0.99 ±0.05 | 1.6×104 ±0.11 | 2.4×10-6 ±0.27×10-6 |
| PEO-4 | 3.77×10-8 ±0.23×10-8 | 1.00 ±0.02 | 9.52×101 ±0.25 | 6.42×10-6 ±0.22×10-6 | 0.91 ±0.03 | 2.09×104 ±0.12 | 1.41×10-6 ±0.17×10-6 | 0.78 ±0.06 | 4.5×104 ±0.14 | 2.0×10-6 ±0.28×10-6 |
| PEO-5 | 7.78×10-7 ±0.21×10-7 | 1.00 ±0.02 | 3.48×101 ±0.19 | 6.82×10-6 ±0.19×10-6 | 0.63 ±0.04 | 1.62×104 ±0.13 | 1.19×10-5 ±0.21×10-5 | 0.91 ±0.04 | 1.4×104 ±0.13 | 5.7×10-5 ±0.22×10-5 |