Table 1. Composition, conductivity, and pH values of the electrolyte used for PEO development.

| Electrolyte | Specimens | TiO2 (g/L) | Conductivity (mS/cm) | pH |
| --- | --- | --- | --- | --- |
| 10.5 gL-1 sodium silicate, 5 gL-1 sodium phosphate dodecahydrate, 2.8 gL-1 potassium hydroxide | A-PEO | 0 | 10.9 | 12.0 |
|  | A-PEO-T2 | 2 | 10.6 | 12.1 |
|  | A-PEO-T5 | 5 | 10.4 | 12.4 |
|  | A-PEO-T10 | 10 | 10.1 | 12.6 |

Table 2.  Parameters of the PEO coatings obtained in studied electrolytes.

Table 3. The elemental composition (at. %) of developed coatings.

| Sample | Contents of elements |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | O | Al | Ti | Si | K |
| A-PEO | 50.0 | 24.6 | 0 | 8.3 | 2.07 |
| A-PEO-T2 | 53.3 | 21.2 | 2.9 | 5.2 | 0.67 |
| A-PEO-T5 | 56.1 | 19.1 | 6.8 | 4.3 | 0.77 |
| A-PEO-T10 | 58.2 | 18.4 | 13.3 | 3.8 | 0.71 |

Table 4. Surface roughness characteristics of the examined materials and thicknesses, both with and without TiO2 electrolyte.

|  | Sa (μm) | Sz (μm) |
| --- | --- | --- |
| A-PEO | 4.1 ± 0.7 | 36.4± 0.7 |
| A-PEO-T2 | 4.8± 0.4 | 39.3± 0.7 |
| A-PEO-T5 | 5.4± 0.6 | 43.6± 0.7 |
| A-PEO-T10 | 6.4± 0.7 | 44.4± 0.7 |

Table 5. The elemental composition (at. %) of developed coatings at three different cross-sectional points from Figure 3.

| A-PEO | O | Al | Ti | Si | K |
| --- | --- | --- | --- | --- | --- |
| Point 1 | 50.4 | 24.6 | 0 | 8.3 | 2.07 |
| Point 2 | 55.3 | 27.2 | 0 | 3.5 | 1.02 |
| Point 3 | 57.6 | 29.2 | 0 | 1.2 | 0.58 |
| A-PEO-T2 | O | Al | Ti | Si | K |
| Point 1 | 53.3 | 21.2 | 2.91 | 5.2 | 1.67 |
| Point 2 | 57.2 | 26.8 | 1.84 | 2.9 | 0.78 |
| Point 3 | 59.1 | 29.4 | 0.83 | 0.99 | 0.45 |
| A-PEO-T5 | O | Al | Ti | Si | K |
| Point 1 | 56.1 | 19.1 | 6.81 | 4.3 | 1.59 |
| Point 2 | 51.4 | 19.6 | 4.72 | 2.7 | 0.74 |
| Point 3 | 47.9 | 23.5 | 1.43 | 0.88 | 0.41 |
| A-PEO-T10 | O | Al | Ti | Si | K |
| Point 1 | 58.2 | 18.4 | 13.3 | 3.80 | 1.36 |
| Point 2 | 53.2 | 19.2 | 9.20 | 2.60 | 0.70 |
| Point 3 | 51.6 | 23.6 | 1.80 | 0.85 | 0.39 |

Table 6. EIS parameters of developed PEO coating on AA2024

| Immersion Time (h) | CPEout Ω-1 cm-2 sα | Rout Ω cm2 | α | CPEin Ω-1 cm-2 sα | Rin Ω cm2 | α |
| --- | --- | --- | --- | --- | --- | --- |
| A-PEO |  |  |  |  |  |  |
| 24 | 2.2×10-6 | 4.8×105 | 0.66 | 7.0×10-6 | 8.2×105 | 0.99 |
| 168 | 2.5×10-5 | 1.5×105 | 0.89 | 5.6×10-6 | 2.8×105 | 0.78 |
| 336 | 4.1×10-5 | 1.8×104 | 0.83 | 3.4×10-5 | 3.9×104 | 0.79 |
| A-PEO-T2 |  |  |  |  |  |  |
| 24 | 3.2×10-6 | 5.9×105 | 0.70 | 1.5×10-6 | 4.8×106 | 0.81 |
| 168 | 5.6×10-5 | 2.5×105 | 0.8 | 6.9×10-6 | 9.4×105 | 0.62 |
| 336 | 9.8×10-5 | 3.7×104 | 0.89 | 4.4×10-5 | 8.1×104 | 0.94 |
| A-PEO-T5 |  |  |  |  |  |  |
| 24 | 2.2×10-6 | 5.5×106 | 0.90 | 5.5×10-6 | 1.6×107 | 0.86 |
| 168 | 1.1×10-6 | 9.4×105 | 0.8 | 2.5×10-6 | 5.6×106 | 0.85 |
| 336 | 9.4×10-5 | 9.2×104 | 0.89 | 3.6×10-5 | 9.8×105 | 0.91 |
| A-PEO-T10 |  |  |  |  |  |  |
| 24 | 6.4×10-6 | 9.4×105 | 0.90 | 1.8×10-6 | 8.7×106 | 0.83 |
| 168 | 3.3×10-6 | 7.3×105 | 0.81 | 2.5×10-6 | 1.1×106 | 0.61 |
| 336 | 4.2×10-5 | 7.1×104 | 0.89 | 4.4×10-5 | 2.9×105 | 0.92 |

Table 7. Constant rate (k) and decomposition rate (χ) of phenol in the presence of developed PEO coatings.

|  | A-PEO-T2 | A-PEO-T5 | A-PEO-T10 |
| --- | --- | --- | --- |
| K [min-1] | 0.0005 | 0.0006 | 0.0008 |
| χ [mM. min-1] | 5.38×10-5 | 6.45×10-5 | 8.94×10-5 |
| R2 | 0.98 | 0.99 | 0.98 |