Table 1. PEO electrolyte and applied conditions.

| Electrolyte | Voltage (V+/V-) [V] | Voltage initial ramp [s] | Frequency [Hz] | Limiting current [mA cm-2] | Time [s] |
| --- | --- | --- | --- | --- | --- |
| 10.5 g L-1 Na2O(SiO2)3·5H2O (CAS: 13729) 5 g L-1 Na3(PO4)·12H2O (CAS: 10101-89-0) 2.8 g L-1 KOH (CAS: 1310-58-3) | 490/-110 (square signal) | 60 | 400 | 100 | 100 |

Table 2. EDS analysis (at.%) of PEO, HSG, and HSG-Ce coatings. Locations are denoted on the top-view SEM micrographs in Figure 4.

| Coating | Location | O | Al | Si | P | C | Ce | Cu |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PEO | 1 | 49.1 | 32.5 | 1.3 | 0.5 | 16.2 | - | 0.4 |
| HSG | 1 | 37.7 | 8.6 | 14.0 | 0.1 | 39.4 | - | 0.2 |
|  | 2 | 48.8 | 24.8 | 3.8 | 0.4 | 22.1 | - | 0.1 |
| HSG-Ce | 1 | 42.8 | 1.9 | 15.6 | - | 39.5 | 0.2 | - |

Table 3. Cross-section EDS analysis (at.%) of PEO, HSG, and HSG-Ce coatings. Locations are denoted on the cross-view SEM micrographs in Figure 5.

| Coating | Location | O | Al | Si | P | C | Cu | Mg | Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PEO | 1 | 39.7 | 15.7 | 0.9 | - | 43.4 | 0.1 | 0.2 | - |
|  | 2 | 36.6 | 37.3 | 0.9 | - | 24.6 | 0.3 | 0.3 | - |
|  | 3 | 22.1 | 49.2 | 0.5 | 2.3 | 24.6 | 0.8 | 0.5 | - |
| HSG | 1 | 22.5 | - | 11.0 | - | 66.4 | 0.1 | - | - |
|  | 2 | 27.4 | 0.4 | 32.5 | - | 39.5 | 0.2 | - | - |
|  | 3 | 36.9 | 4.6 | 17.5 | - | 40.9 | 0.1 | - | - |
|  | 4 | 46.5 | 23.2 | 5.8 | - | 24.0 | 0.2 | 0.3 | - |
|  | 5 | 30.2 | 41.4 | 4.0 | - | 23.0 | 0.8 | 0.6 | - |
| HSG-Ce | 1 | 28.4 | - | 10.4 | - | 61.0 | 0.1 | - | 0.1 |
|  | 2 | 24.6 | 0.3 | 31.1 | - | 43.2 | 0.3 | - | 0.5 |
|  | 3 | 31.4 | 1.6 | 23.0 | - | 43.2 | 0.3 | - | 0.5 |
|  | 4 | 37.8 | 11.9 | 12.6 | - | 37.2 | 0.2 | 0.1 | 0.2 |
|  | 5 | 39.7 | 30.9 | 2.6 | - | 25.9 | 0.5 | 0.4 | - |

Table 4. Roughness values of studied PEO, HSG, and HSG-Ce coatings on the 2024-T3 alloy.

| Coating | Sa (µm) | S10z (µm) |
| --- | --- | --- |
| PEO | 0.31 ± 0.03 | 6.2 ± 2.0 |
| HSG | 0.26 ± 0.01 | 3.8 ± 0.3 |
| HSG-Ce | 0.29 ± 0.01 | 3.4 ± 0.3 |

Table 5. Fitted electrical parameters of studied coatings after 1 h and 21 days of immersion in 3.5 wt.% NaCl solution.

| Coating | CPE-1 | n-1 | R-1 | CPE-2 | n-2 | R-2 | CPE-3 | n-3 | R-3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 hour |  |  |  |  |  |  |  |  |  |
| PEO | 1.5·10-7 (±5·10-8) | 0.73 (±0.01) | 4.2·106 (±7·105) | 5.2·10-8 (± 2·10-9) | 0.90 (±0.01) | 1.70·104 (±4·103) | - | - | - |
| HSG | 1.7·10-7 (±3·10-8) | 0.48 (±0.09) | 2.8·106 (±3·105) | 8.5·10-8 (± 6·10-9) | 0.86 (±0.03) | 5.0·104 (±1·103) | 2.3·10-8 (±2·10-9) | 0.88 (±0.04) | 1.66·104 (±2·103) |
| HSG-Ce | 6.3·10-8 (±8·10-9) | 0.53 (±0.03) | 2.1·107 (±2·106) | 2.6·10-8 (± 5·10-9) | 0.88 (±0.02) | 8.2·105 (±2·104) | 4.6·10-9 (±1·10-10) | 0.98 (±0.01) | 5.4·104 (±3·103) |
| 21 days |  |  |  |  |  |  |  |  |  |
| PEO | 1.6·10-4 (±4·10-5) | 0.73 (±0.07) | 2.5·105 (±2·104) | 5.0·10-5 (±8·10-6) | 0.87 (±0.01) | 1.6·104 (±4·103) | - | - | - |
| HSG | 9.9·10-7 (±8·10-8) | 0.71 (±0.02) | 5.7·106 (±8·105) | 4.4·10-7 (±8·10-8) | 0.81 (±0.01) | 2.8·104 (±2·103) | 1.5·10-7 (±4·10-8) | 0.77 (±0.01) | 7.0·103 (±1·102) |
| HSG-Ce | 1.2·10-7 (±7·10-8) | 0.70 (±0.01) | 8.0 ·107 (±1·106) | 3.1·10-8 (±5·10-9) | 0.83 (±0.04) | 8.3·104 (±1·103) | 1.6·10-8 (±6·10-9) | 0.90 (±0.03) | 3.0·103 (±1·102) |
| + Units: CPE: F s(n-1)·cm-2; R: cm2 |  |  |  |  |  |  |  |  |  |

Table 6. EDS analysis (at.%) of PEO, HSG, and HSG-Ce coatings after 21 days of immersion in 3.5 wt.% NaCl aqueous solution. Locations are denoted on the top-view SEM micrographs in Figure 10.

| Coating | Location | O | Al | Si | Na | C | Cu | Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PEO | 1 | 52.6 | 34.4 | 0.9 | - | 11.1 | 1.0 | - |
| HSG | 1 | 45.0 | 17.8 | 8.0 | - | 29.0 | 0.2 | - |
|  | 2 | 47.7 | 35.1 | 1.3 | - | 15.4 | 0.5 | - |
|  | 3 | 41.7 | 11.1 | 13.1 | - | 33.9 | 0.2 | - |
| HSG-Ce | 1 | 44.2 | 11.5 | 11.5 | 0.5 | 31.9 | 0.2 | 0.2 |
|  | 2 | 16.9 | 68.1 | 12.4 | - | - | 2.6 | - |
|  | 3 | 41.8 | 2.9 | 15.1 | 0.5 | 39.4 | - | 0.3 |

Table 7. EDS analysis (at.%) of PEO, HSG, and HSG-Ce scribed coatings after 11 and 21 days immersion in 3.5 wt.% NaCl aqueous solution. Locations are denoted on the top-view SEM micrographs in Figure 10.

| Coating | Location | O | Al | Si | Na | C | Cu | Mg | Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 days |  |  |  |  |  |  |  |  |  |
| PEO | 1 | 52.4 | 29.1 | 2.4 | 1.2 | 13.9 | 1.0 | - |  |
| HSG | 1 | 44.7 | 15.7 | 8.6 | 1 | 29.6 | 0.4 |  |  |
|  | 2 | 46.1 | 10.8 | 10.3 | 1.3 | 31.1 | 0.4 |  |  |
|  | 3 | 47.7 | 27.1 | 5.8 | 3.6 | 14.6 | 1.2 |  |  |
| HSG-Ce | 1 | 9.6 | 72.4 | 1.9 | - | - | 15.8 |  | 0.3 |
|  | 2 | 41.4 | 12.8 | 13.3 | 1.0 | 30.4 | 0.7 |  | 0.4 |
| 21 days |  |  |  |  |  |  |  |  |  |
| PEO | 1 | 52.4 | 29.1 | 2.4 | 1.2 | 13.9 | 1.0 | - |  |
|  | 2 | 53.3 | 25.9 | 2.5 | 1.0 | 15.2 | 1.8 | 0.3 |  |
|  | 3 | 50.0 | 28.2 | 2.5 | 0.8 | 15.2 | 2.9 | 0.4 |  |
|  | 4 | 53.7 | 30.4 | 1.8 | 0.2 | 12.5 | 1.0 | 0.4 |  |
| HSG | 1 | 46.1 | 16.1 | 8.1 | 1.1 | 28.2 | 0.4 |  |  |
| HSG-Ce | 1 | 44.3 | 23.6 | 5.3 | 3.9 | 20.2 | 2.7 |  | - |
|  | 2 | 52.0 | 15.9 | 9.2 | 1.5 | 20.7 | 0.3 |  | 0.4 |
|  | 3 | 56.1 | 25.6 | 2.4 | 1.3 | 13.2 | 1.2 |  | 0.2 |
|  | 4 | 44.0 | 16.5 | 10.0 | 0.9 | 28.4 | - |  | 0.2 |