Table 1. Surface characteristics (thickness, contact angle, roughness measurements) of the studied coatings from Figure 8.

| System | Average pore size (μm) | Sa (μm) | Thickness (μm) | Contact angle (o) |
| --- | --- | --- | --- | --- |
| Mg3Zn0.4Ca/PEO | 0.3 ± 0.1 | 4.2 ± 0.2 | 7.8 ± 0.8 | 23.5 ± 0.8 |
| Mg3Zn0.4Ca/PEO/PLA | 10 ± 1.1 | 3.1 ± 0.2 | 36.0 ± 1.2 | 95.0 ± 1.1 |
| Mg3Zn0.4Ca/PEO/PCL | 7 ± 1.9 | 2.5 ± 0.5 | 28.0 ± 0.4 | 94.4 ± 2.3 |

Table 2. EDS analysis (% at.) of PLA and PCL-coated samples on Mg3Zn0.4Ca alloy from Figure 13 (c, e).

| Specimen | Location |  | O | Na | Mg | Si | P | Cl | K | Ca | Zn | Ca/P |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mg3Zn0.4Ca/HHC-PLA |  | 1 | 75.9 | 3.0 | 18.1 | 0.2 | 0.6 | 0.4 | 0.0 | 1.2 | 0.6 | 2.00 |
|  |  | 2 | 77.7 | 1.1 | 16.8 | 0.1 | 1.0 | 0.1 | 0.1 | 2.3 | 1.0 | 2.29 |
|  |  | 3 | 78.4 | 1.7 | 15.8 | 0.0 | 0.9 | 0.4 | 0.0 | 2.0 | 0.6 | 2.20 |
| Mg3Zn0.4Ca/HHC-PCL |  | 4 | 88.7 | 0.4 | 3.3 | 3.7 | 1.2 | 0.8 | 0.0 | 1.7 | 0.0 | 1.33 |
|  |  | 5 | 78.5 | 1.1 | 8.5 | 0.2 | 4.3 | 0.4 | 0.2 | 6.3 | 0.4 | 1.47 |
|  |  | 6 | 79.0 | 1.5 | 8.3 | 0.3 | 3.8 | 0.5 | 0.3 | 5.8 | 0.8 | 1.53 |
|  |  | 7 | 73.2 | 1.1 | 9.4 | 0.2 | 5.1 | 0.4 | 0.0 | 8.0 | 2.9 | 1.57 |