Compressive strength of masonry made of clay bricks and cement mortar: an estimation based on neural networks and fuzzy logic

Julio Garzón-Rocaa, Creu Obrer Marcoa, Jose M. Adama,*

aICITECH, Departamento de Ingeniería de la Construcción y Proyectos de Ingeniería Civil, Universitat Politècnica de València, Camino de Vera s/n, 46071, Valencia, Spain

* Corresponding author: Tel.: +34 963877562; fax: +34 963877568

E-mail address: joadmar@cst.upv.es

ABSTRACT

The use of mathematical tools such as Artificial Neural Networks and Fuzzy Logic has been shown to be useful for solving complex engineering problems, without the need to reproduce the phenomenon under study, when the only information available consists of the parameters of the problem and the desired results. Based on a collection of 96 laboratory tests, this paper uses Artificial Neural Networks and Fuzzy Logic to determine the compressive strength of a masonry structure composed of clay bricks and cement mortar, by using only two parameters: the compressive strength of the mortar and that of the bricks. These mathematical techniques are an alternative to the complex analytical formulas dependent on a large number of parameters and to empirical formulas, which, even though simple, often give unrealistic values. The results obtained are compared to the calculation methods proposed by other authors and other standards and demonstrate the suitability of using Neural Networks and Fuzzy Logic to predict the compressive strength of masonry.

Keywords: neural networks, fuzzy logic, masonry, compressive strength

1. Introduction

A great number of parameters come into play in the compressive strength of clay brick masonry walls joined together by cement mortar. In general, it can be said that the resistance mechanism of masonry subjected to compression loads depends basically on the interaction between the bricks and the mortar. The characteristics of the materials themselves (bricks and mortar) also differ when they are acted upon in isolation and when they are the components of a masonry wall. It should also be borne in mind that masonry is an anisotropic element and highly sensitive to building processes. The wide range of existing parameters, some quantitative (e.g. brick compressive strength) and others more qualitative (e.g. construction process) greatly complicate the calculations and design of masonry structures.

Different analytical models [1–5] have been proposed to determine the compressive strength of masonry structures. These try to obtain the compressive strength of the brick and mortar combination from theoretical principles, starting from a series of mechanical hypotheses and applying equilibrium and compatibility equations. Although most of these models assume that the bond between bricks and mortar remains intact when either brick or mortar fails, it has been shown that this is not completely correct [6]. The models are also highly complex, require a variety of parameters (geometry, brick and mortar and compressive strengths, elasticity modulus and Poisson coefficient) and obtain expressions in which some of the factors are interrelated. Another approach is the use of empirical models [7] obtained from different experimental studies, composed of simple expressions, most of which use two easily obtainable parameters: the compressive strength of the mortar (fm) and that of the brick (fb). The simplicity of these models is such that the design proposals of various codes such as Eurocode 6 [12], the ACI Standard 530.99 [13] and the British Standard BD 21/93 [14] are in fact empirical expressions largely dependent on the parameters fm and fb.

As an alternative to the empirical models, this paper aims to determine the compressive strength of a masonry structure formed by clay bricks and cement mortar by means of two numerical techniques, Artificial Neural Networks and Fuzzy Logic, both of which obtain the solution to a complex problem starting from the system’s input and output data and without considering the physical phenomenon modeled. Neural Networks have recently been used to solve different engineering problems such as predicting the shear strength of RC beams [15] and columns [16], simulating the size effect on shear strength of RC beams without stirrups [17], modeling reinforced fibrous concrete corbels without stirrups [18] or predicting steel-concrete bonds [19]. Fuzzy Logic has been shown to be useful in problems like active seismic response control systems [20], assessment of reinforced concrete building structures [21], predicting the moment capacity of ferrocement members [22] and estimating the service life of reinforced concrete structural members in corrosive environments [23].

After applying the Artificial Neural Networks and Fuzzy Logic methods, the results obtained are compared with several empirical proposals in order to demonstrate their reliability.

2. Recopilación de ensayos experimentales

The first step in both the Artificial Neural Network (ANN) and the fuzzy inference system is to identify the parameters to be entered in the model. According to the empirical models [7–11] and most of the codes [12–14] there are two basic parameters that define the compression strength of a masonry structure: mortar compressive strength (fm) and brick compression strength (fb).  These two parameters thus form the input of both the Neural Network and the fuzzy system. The output, i.e. the desired result, is the compressive strength of the masonry structure (f).

After identifying inputs and outputs, a review was made of 96 experimental studies [4,6,10,24–39] (see Table 1) in all of which the masonry structure is formed of clay bricks and cement mortar and the aim is to determine the compressive strength of the bricks and mortar combination (f). The working variables (inputs) are the mortar (fm) and brick compressive strength (fb). Table 2 presents the range of maximum and minimum values and some statistical parameters (mean, standard deviation and coefficient of variance) of each variable used in the study.

3. Neural Network modeling

An Artificial Neural Network (ANN) consists of a set of interconnected elements called neurons that provide a response or output from a series of inputs. Their operating system is shown in Fig. 1. Inputs are combined linearly and each input is multiplied by a coefficient known as the weight and is then given an independent term or bias. The result of the linear combination is applied to a function that may be either linear or non-linear, called the activation function or transfer function, which provides the neuron’s output.

Table 1

Experimental data used for training and testing ANN and Fuzzy Logic.

| Test | fm (MPa) | fb (MPa) | f (MPa) | Ref. |  | Test | fm (MPa) | fb (MPa) | f (MPa) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 3.40 | 101.70 | 29.90 | [24] |  | 49 | 2.63 | 76.53 | 32.47 | [10] |
| 2 | 13.70 | 101.70 | 32.50 | [24] |  | 50 | 2.63 | 76.53 | 32.53 | [10] |
| 3 | 26.40 | 101.70 | 40.90 | [24] |  | 51 | 2.63 | 76.53 | 35.09 | [10] |
| 4 | 52.60 | 101.70 | 48.20 | [24] |  | 52 | 14.20 | 61.02 | 36.54 | [10] |
| 5 | 3.20 | 26.90 | 11.00 | [4] |  | 53 | 14.20 | 61.02 | 35.56 | [10] |
| 6 | 12.70 | 26.90 | 14.50 | [4] |  | 54 | 14.20 | 61.02 | 40.42 | [10] |
| 7 | 6.10 | 13.10 | 5.40 | [25] |  | 55 | 14.20 | 61.02 | 36.97 | [10] |
| 8 | 9.90 | 17.00 | 7.30 | [26] |  | 56 | 14.20 | 61.02 | 42.90 | [10] |
| 9 | 15.20 | 25.50 | 9.30 | [27] |  | 57 | 14.20 | 61.02 | 38.61 | [10] |
| 10 | 0.50 | 10.00 | 2.00 | [28] |  | 58 | 16.61 | 61.02 | 40.10 | [10] |
| 11 | 41.03 | 94.25 | 87.06 | [10] |  | 59 | 15.00 | 61.02 | 28.57 | [10] |
| 12 | 41.03 | 94.25 | 86.81 | [10] |  | 60 | 15.00 | 61.02 | 31.71 | [10] |
| 13 | 41.03 | 94.25 | 87.57 | [10] |  | 61 | 3.10 | 8.20 | 2.30 | [29] |
| 14 | 19.04 | 94.25 | 60.41 | [10] |  | 62 | 5.00 | 14.90 | 8.50 | [30] |
| 15 | 19.04 | 94.25 | 59.39 | [10] |  | 63 | 15.70 | 34.00 | 15.60 | [31] |
| 16 | 18.42 | 94.25 | 60.35 | [10] |  | 64 | 14.70 | 19.90 | 9.90 | [32] |
| 17 | 8.19 | 94.25 | 47.09 | [10] |  | 65 | 11.40 | 19.90 | 13.50 | [32] |
| 18 | 8.19 | 94.25 | 45.62 | [10] |  | 66 | 10.60 | 10.70 | 3.20 | [6] |
| 19 | 8.19 | 94.25 | 46.77 | [10] |  | 67 | 7.30 | 10.70 | 2.10 | [6] |
| 20 | 8.58 | 94.25 | 50.45 | [10] |  | 68 | 4.10 | 10.70 | 2.90 | [6] |
| 21 | 8.58 | 94.25 | 54.38 | [10] |  | 69 | 4.20 | 10.70 | 2.50 | [6] |
| 22 | 8.58 | 94.25 | 47.15 | [10] |  | 70 | 0.45 | 18.60 | 5.13 | [33] |
| 23 | 2.54 | 94.25 | 31.48 | [10] |  | 71 | 1.41 | 18.60 | 5.83 | [33] |
| 24 | 2.54 | 94.25 | 34.84 | [10] |  | 72 | 1.45 | 18.60 | 6.68 | [33] |
| 25 | 2.63 | 94.25 | 34.90 | [10] |  | 73 | 1.34 | 18.60 | 5.60 | [33] |
| 26 | 45.38 | 94.25 | 92.14 | [10] |  | 74 | 1.58 | 18.60 | 5.38 | [33] |
| 27 | 45.38 | 94.25 | 76.91 | [10] |  | 75 | 1.42 | 18.60 | 5.53 | [33] |
| 28 | 45.38 | 94.25 | 85.28 | [10] |  | 76 | 3.00 | 66.00 | 11.70 | [34] |
| 29 | 36.26 | 94.25 | 92.90 | [10] |  | 77 | 3.10 | 17.70 | 4.00 | [9] |
| 30 | 36.26 | 94.25 | 85.03 | [10] |  | 78 | 3.10 | 16.10 | 2.90 | [9] |
| 31 | 36.26 | 94.25 | 101.27 | [10] |  | 79 | 3.10 | 28.90 | 5.10 | [9] |
| 32 | 35.87 | 94.25 | 89.60 | [10] |  | 80 | 3.10 | 20.60 | 4.30 | [9] |
| 33 | 35.87 | 94.25 | 85.03 | [10] |  | 81 | 20.60 | 17.70 | 7.40 | [9] |
| 34 | 33.94 | 94.25 | 86.81 | [10] |  | 82 | 20.60 | 16.10 | 6.50 | [9] |
| 35 | 9.98 | 94.25 | 51.66 | [10] |  | 83 | 20.60 | 28.90 | 8.50 | [9] |
| 36 | 9.98 | 94.25 | 53.94 | [10] |  | 84 | 20.60 | 20.60 | 7.60 | [9] |
| 37 | 9.98 | 94.25 | 55.97 | [10] |  | 85 | 15.20 | 17.70 | 6.50 | [9] |
| 38 | 9.33 | 94.25 | 51.53 | [10] |  | 86 | 15.20 | 16.10 | 5.90 | [9] |
| 39 | 9.33 | 94.25 | 52.10 | [10] |  | 87 | 15.20 | 28.90 | 7.20 | [9] |
| 40 | 9.33 | 94.25 | 50.18 | [10] |  | 88 | 15.20 | 20.60 | 6.80 | [9] |
| 41 | 7.82 | 94.25 | 43.15 | [10] |  | 89 | 10.00 | 20.80 | 14.33 | [35] |
| 42 | 7.82 | 94.25 | 50.38 | [10] |  | 90 | 9.20 | 13.80 | 13.50 | [36] |
| 43 | 7.82 | 94.25 | 51.15 | [10] |  | 91 | 7.00 | 13.80 | 13.20 | [36] |
| 44 | 39.26 | 76.53 | 56.55 | [10] |  | 92 | 13.10 | 19.70 | 13.50 | [37] |
| 45 | 40.43 | 76.53 | 58.50 | [10] |  | 93 | 10.00 | 19.70 | 13.20 | [37] |
| 46 | 8.19 | 76.53 | 39.58 | [10] |  | 94 | 2.30 | 30.50 | 7.50 | [37] |
| 47 | 8.34 | 76.53 | 39.04 | [10] |  | 95 | 7.10 | 9.60 | 3.00 | [38] |
| 48 | 8.34 | 76.53 | 40.38 | [10] |  | 96 | 1.00 | 55.00 | 12.10 | [39] |

Table 2

Statistics of experimental data

| Variable | Maximum (MPa) | Minimum (MPa) | Mean (MPa) | Standard deviation (MPa) | COV (%) |
| --- | --- | --- | --- | --- | --- |
| fm | 52.60 | 0.45 | 14.16 | 12.77 | 0.90 |
| fb | 101.70 | 8.20 | 57.79 | 35.12 | 0.61 |
| f | 101.27 | 2.00 | 33.60 | 27.75 | 0.83 |

The feedforward multilayer perceptron network is an ANN consisting of a series of neurons distributed into three or more layers, (see Fig. 2). Each of the neurons belonging to one of these layers is completely connected to all the neurons in the previous and following layers, although there are no connections between neurons in the same layer. The first layer is the input layer, i.e. the ANN input parameters and contains the same number of neurons as inputs. The last is the output layer i.e. the ‘‘results’’ of the ANN, with the same number of neurons as problem outputs. The layer or layers between these two are known as the hidden layers. The number of hidden layers and the number of neurons in each hidden layer depend on the problem under study and cannot be known beforehand.

Fig. 1. Single neuron work.

Fig. 2. Feedforward Neural Network.

In order to operate an ANN, the network must first be ‘‘trained’’. For this a number of examples must be available consisting of data in which both their inputs and the corresponding outputs are known. The aim is for the network to learn the functional relationship between the input and output variables, thus obtaining the different weights and biases. The back-propagation algorithm is one of the most frequently used methods of training a feedforward multilayer perceptron network. It starts out from a series of random weights and executes the network with the examples provided, obtaining a value for the output which will be different from its real value. The error between the output obtained by the network and the real output is propagated backwards in order to modify the weight and bias values. This process is repeated until the error has been reduced to a pre-set value or until the maximum number of iterations or epochs has been reached.

3.1. Network architecture

The Matlab commercial software [40], especially the Neural Network Toolbox, was used in this work to define a 2-n-1 feedforward multilayer perceptron network. This ANN has two input parameters, mortar compressive strength (fm) and brick compressive strength (fb), an output value, the masonry compressive strength (f), and a hidden layer with n neurons. Since there is no generally accepted standard in the literature as to the number of neurons that should be contained in the hidden layer, this number is usually determined by trial and error. In this study we defined six ANN and varied the number of neurons in the hidden layer (n) from 1 to 6 and then selected the ANN considered to give the best results.

The hidden layer activation function was the sigmoid function g(x) = 1/(1+e-x), while the output layer contained a linear neuron. This combination makes it possible for the network to learn both the linear and non-linear relationships between the input and output vectors [40]. The Lavenberg–Marquardt algorithm [40] with back-propagation and 2000 epochs was used the network training.

3.2. Network data preparation

From the data of the total of 96 studies (see Section 2), 80% (76 data sets) were used to train the network and the remaining 20% (20 data sets) were used for testing. The data were not entered directly in the ANN but were previously scaled in order to improve the stability of the training process and to obtain a higher degree of accuracy. Since the sigmoid function varies between 0 and 1, being asymptotic for these values, both input and output values were scaled in the 0.1–0.9 range [17] by a simple linear normalization function:

(1)

where Xi and Xi,ANN are the input or output value before and after being scaled, and Xmin and Xmax the minimum and maximum value of the input or output value to be scaled.

3.3. Neural Network simulations

Table 3 shows the results of the six ANNs carried out. Each one obtained: the maximum, minimum, mean and standard deviation of the ratio between the masonry compressive strength according to the reviewed experimental studies (fEXP) and that obtained from the ANN (fANN); the Pearson coefficient (R) of the correlation and the Mean Square Error (MSE). As can be observed, the ANN with the 2–5–1 architecture achieved the best performance for the test set, with a minimum and maximum value of fEXP/fANN close to 1, a mean fEXP/fANN of 1.005, a standard deviation less than 0.15 and good values for both MSE and R coefficient. For this ANN, the weight matrix and bias are:

for the hidden layer, and:

for the output layer.

Table 3

ANN results

| ANN | Training |  |  |  |  |  |  | Test |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Min. | Max. | Mean | Std. | R | MSE |  | Min. | Max. | Mean | Std. | R | MSE |
| 2-1-1 | 0.608 | 1.414 | 1.001 | 0.176 | 0.947 | 0.0045 |  | 0.586 | 1.484 | 0.994 | 0.202 | 0.955 | 0.0060 |
| 2-2-1 | 0.598 | 1.404 | 1.003 | 0.161 | 0.966 | 0.0033 |  | 0.636 | 1.705 | 1.014 | 0.214 | 0.989 | 0.0014 |
| 2-3-1 | 0.616 | 1.296 | 1.001 | 0.140 | 0.979 | 0.0021 |  | 0.685 | 1.349 | 0.993 | 0.161 | 0.970 | 0.0027 |
| 2-4-1 | 0.636 | 1.352 | 1.003 | 0.120 | 0.986 | 0.0015 |  | 0.789 | 1.341 | 1.010 | 0.138 | 0.983 | 0.0011 |
| 2-5-1 | 0.626 | 1.372 | 1.004 | 0.150 | 0.978 | 0.0021 |  | 0.773 | 1.192 | 1.005 | 0.149 | 0.985 | 0.0021 |
| 2-6-1 | 0.713 | 1.362 | 1.000 | 0.115 | 0.991 | 0.0007 |  | 0.828 | 1.999 | 1.076 | 0.241 | 0.989 | 0.0023 |
| Minimum (Min), Maximum (Max), Mean and Standard deviation (Std) are related to the ratio fEXP/fANN |  |  |  |  |  |  |  |  |  |  |  |  |  |

3.4. Design proposal from ANN 2-1-1

Although the ANN with the best performance had 5 neurons in the hidden layer, the 2–1–1 network with only a single hidden neuron also gave good results, presenting a test set with a mean value of 0.99 and a standard deviation of 0.20 (besides high R and low MSE values). Since this network only has one hidden neuron, it is a simple task to obtain an expression that can be applied directly without the need to construct a mathematical Neural Network. The weight matrices and bias of this ANN are:

Bearing in mind that the activation function for the hidden layer was a sigmoid and the activation function for the output layer was linear, the expression that determines the compressive strength of the masonry structure will be:

(2)

where f*m and f*b are the values fm and fb, although scaled in accordance with Eq. (1) and using the values given in Table 2; the value of f⁄ will also be the value of the compressive strength of the element scaled between 0.1 and 0.9. Eq. (1) and Table 2 will again have to be used, although in this case solving Eq. (1) in reverse, to obtain the value of f. Applying the conditions given above, Eq. (3) can be reached by operating as required and rounding off the values, which will give the value of the compressive strength of the masonry structure, given that of the bricks and mortar.

(3)

Applying Eq. (3) directly to the 96 data sets, a mean value of the fEXP/fANN ratio of 1.02 was obtained with a standard deviation of 0.35. It should be pointed out that this expression can only be used if the fm, fb and f values are within the range studied. Eq. (3) can therefore be applied if the following expression is complied with: 0.5 MPa < fm < 52 MPa; 8 MPa < fb < 101 MPa; 2 MPa < f < 101 MPa.

4. Fuzzy Logic

Fuzzy set theory, proposed by Zadeh [41], is a mathematical tool that allows work to be carried out in an uncertain environment. As opposed to classical logic, in which an element belongs (1) or does not belong (0) to a set, a fuzzy set is a set without a crisp, clearly defined boundary [40], i.e., it can contain elements with only a partial degree of membership (a number between 0 and 1). In Fuzzy Logic, therefore, a function known as a membership function is defined for each set that gives an idea of the degree to which each of the studied elements belongs to the set. This membership function may take many forms, although the most frequently used are triangular, trapezoidal, polynomial or Gaussian.

When working with Fuzzy Logic, if-then type rules are used to formulate conditional statements. A single fuzzy if-then rule assumes the form: “if x is A then y is B”, where A and B are values of a fuzzy set and x and y are the variables of the problem [40]. The if-then rules may be made more complex by introducing logical operators such as “and”  or  “or”.

Fuzzy inference is the process of formulating the mapping from a series of given input values to an output value using Fuzzy Logic [40]. In 1985 Sugeno [40] introduced a fuzzy inference method, in which the result of the if-then rules is always either linear or constant. A typical rule in a Sugeno fuzzy model has the form: “If input 1 = x and input 2 = y, then output is z = ax + by + c”. For each rule the obtained output zi is weighted by the firing strength wi of the rule [40]. Finally, the final output (ofinal) of the system is the weighted average of all rule outputs, computed as:

(4)

4.1. Fuzzy logic application

The Matlab Fuzzy Logic Toolbox [40] was used to find a Sugeno fuzzy inference system that could be used to determine the compressive strength of a masonry structure (f) when its brick (fb) and mortar (fm) compressive strengths are already known. This tool provides a membership function, the if-then rules and the weight wi that define the Sugeno fuzzy inference system and provide the relationships between a series of inputs and the output. A total of 96 data sets were used, taken from the experimental studies reviewed (see Section 2).

4.2. Matlab Fuzzy Logic Toolbox Operation

The following is a brief description of how the Matlab Fuzzy Logic Toolbox [40] operates to determine the membership function, the if–then rules and the weights (wi) that define a Sugeno fuzzy inference system.

The program first analyses the data entered and for each input variable (in this case fm and fb) proposes a number of fuzzy sets, for which it also proposes an associated membership function. These operations are carried out without any importance being given to the physical significance of the variables, but are simply confined to the numerical values entered. For example, the program could decide that there are three sets for fb of low, medium and high compressive strengths. After defining the sets, the program then considers a series of if–then rules in which it combines the sets and solves a number of linear functions (the output of the Sugeno fuzzy inference system) dependent on the input variables associated with each of the if-then rules. Lastly, it calculates the final output according to Eq. (4).

The membership function, the if–then rules and the linear functions defined in the program’s first solution can sometimes be improved on. In order to check this, Matlab [40] allows the results obtained (final output) to be compared to the results entered in the program as output (the real values of f). If it is then thought the results can be improved on, it allows the user to modify the parameters that the program had activated by default, such as the if–then rules or the shape of the membership function (rectangular, triangular or Gaussian). The program then re-defines the solution and repeats the process until the Sugeno fuzzy inference system is considered to be the optimum.

4.3. Fuzzy logic results

Applying the method described above, a Sugeno Fuzzy Logic inference system was obtained that was able to determine the compressive strength of a masonry structure (f) from the mortar’s

compressive strength (fm) and that of the bricks (fb). In the case of the fm variable, Matlab [40] identified four fuzzy sets with the membership functions shown in Fig. 3a, expressed as:

(5)

In which j represents the fuzzy set and λ has a value of: 9.90 for fuzzy set 1; 8.58 for fuzzy set 2; 41.03 for fuzzy set 3; and 14.20 for fuzzy set 4.

Three fuzzy sets were identified for the fb variable with the membership functions as shown in Fig. 3b, expressed as:

(6)

In which j represents the fuzzy set and λ has a value of: 17.10 for fuzzy set 1; 94.25 for fuzzy set 2; and 61.02 for fuzzy set 3.

Four if-then rules were also defined:

(7)

(8)

(9)

(10)

The weights (wi) for each if-then rule were assumed to be equal to 1.

Using the fuzzy inference system described above, a mean value of the fEXP/fFL ratio was obtained, i.e. masonry compressive strength from the experimental tests (fEXP) over the compressive strength calculated by Fuzzy Logic (fFL), with a value of 1.09 and standard deviation of 0.34, the maximum and the minimum value of the ratio being 2.32 and 0.37, respectively.

Fig. 3. Membership functions: (a) input fm; and (b) input fb.

Fig. 4 shows a diagram of the fuzzy inference system. As can be seen, f shows a general tendency to rise with increases in fm and fb, but when the mortar compressive strength (fm) goes beyond approximately 35 MPa the value of f starts to fall. Also, the strength of the structure (f) usually lies between fb and fm. However, when fm reaches values higher than half that of fb, it then starts to drop below the values of fm and fb. Finally, it should be pointed out that even though points can be seen in Fig. 4 with f < 0, this is entirely due to the fact that they are in a zone with no available input data, since in practice there are very few masonry structures in which the compressive strength of the materials corresponds to the values in these zones (very high fm y and very low fb).

Fig. 4. Graph of the results obtained from a Sugeno fuzzy inference system.

5. Comparación de los resultados obtenidos con los métodos de cálculo

In order to study the degree of fit between the value of the compressive strength of masonry structures by ANN and Fuzzy Logic as compared to empirical methods, we compared our results with six proposed empirical calculation methods:

(a) Mann [7]: after a series of 925 tests, this author proposed the following expression:

(11)

(b) Dayaratnam [8]: after some tests carried out in India, this author proposed the expression:

(12)

(c) Kaushik et al. [9]: in this study the authors tested different types of bricks with different mortar mixes and obtained the following expression:

(13)

(d) Dymiotis et al. [10]: these authors applied regression analysis to a selection of existing tests and obtained a series of second-degree equations to be applied according to the fm, fb values, height of the bricks, mortar density, total height of the bricks and mortar structure and total brick volume. When the only data available refer to the strengths of the mortar and bricks, the expression applied is:

(14)

(e) Eurocode 6 [12]: according to this standard, the value of f can be obtained from:

(15)

K being a coefficient varying between 0.4 and 0.7 that depends on the characteristics of the bricks and mortar and the building methods used in the masonry structure. To apply this expression, the following conditions must be complied with: fm < 20 MPa and fm < 2·fb.

(f) ACI 530.99 [13]: based on experiments carried out in the US, proposes the following expression:

(16)

with the restriction that mortar thickness must be less than 16 mm.

The above proposals were applied to the 96 data sets reviewed (see Section 2) to obtain the ratio between the real compressive strength of the masonry structure and the value obtained from each of the proposals. Table 4 shows the mean value and standard deviation of this ratio for each of the proposals, together with the values obtained from the ANN and Fuzzy Logic. A multiple linear regression analysis was also performed on the 96 data sets and the following expression was obtained:

(17)

As can be seen in Table 4, the results of the multiple linear regression are not good and clearly show that the relationship between fb and fm with f is non-linear. This formulation is therefore not a valid method of estimating the compressive strength of masonry structures. As regards the different calculation proposals, apart from Mann’s [7] in which the mean value of the fproposed/freal ratio is higher than 1, all the empirical expressions are firmly on the safe side and many have mean values less than 0.50. The Dymiotis et al. [10] and Mann [7] proposals come closest to 1, both remaining at a distance of 0.19, below 1 in the former case and over 1 in the latter. The standard deviation values were not low, with a value of 0.3 in all cases except those of Mann [10] and Dayaratnam [8]. The comparison of the empirical proposals with the results obtained by ANN and Fuzzy Logic in this study shows that our proposed method is an improvement on the existing expressions. The numerical techniques we used obtained a mean value fairly close to 1, with a standard deviation similar to that of the empirical expressions. Lastly, if a comparison is made between the statistics of Eq. (3) in the present study with the statistics from the reviewed empirical expressions [7–10,12,13], it can be concluded that our proposal is a considerable improvement and could therefore be safely recommended for use by researchers and practitioners interested in determining the compressive strength of a masonry structure.

Table 4

Comparison between empirical methods, ANN and Fuzzy Logic

| Proposal | Mean | Standard deviation |
| --- | --- | --- |
| Mann [7] | 1.19 | 0.22 |
| Dayaratnam [8] | 0.32 | 0.22 |
| Kaushik et al. [9] | 0.48 | 0.34 |
| Dymiotis et al. [10] | 0.79 | 0.37 |
| Eurocode 6 [12] | 0.57 | 0.34 |
| ACI 530.99 [13] | 0.29 | 0.32 |
| Design Proposal from ANN 2-1-1 | 1.02 | 0.35 |
| Fuzzy Logic | 1.09 | 0.34 |
| Linear regression | 1.22 | 1.52 |

8. Conclusions

From the data collected from a review of 96 experimental studies in this study we used the numerical techniques of Artificial Neural Networks and Fuzzy Logic to determine the compressive strength of a masonry structure composed of clay bricks and cement mortar, of which only the compressive strengths of the bricks and cement were known.

The results of applying the Artificial Neural Network proved to be highly satisfactory, with mean values of the real/estimated compressive strength ratio close to 1 and relatively low standard deviation. It was also possible to obtain from this model an expression (Eq. (3)) that allowed the compressive strength of a masonry structure to be calculated directly, without the need to program an Artificial Neural Network.

The application of Fuzzy Logic was also shown to give good results, with a mean value of the real/estimated compressive strength ratio of 1.09 and standard deviation at 0.3. This technique also showed that in general the compressive strength of a masonry structure increases when the compressive strength of the bricks and mortar is raised and normally lies somewhere between these two values.

Finally, the results obtained from our study were compared to four proposals by other authors (Mann [7], Dayaratnam [8], Kaushik et al. [9] and Dymiotis et al. [10]), the Eurocode 6 [12] and ACI 530.99 [13] standards, and were subjected to a multiple linear analysis. These comparisons showed that the different proposals do not closely agree with the experimental results, with an average discrepancy of around 20% with the real value, which demonstrates the suitability of applying tools such as Neural Networks and Fuzzy Logic, which have been shown to achieve good agreement with experimental results.

Acknowledgements

The authors wish to express their gratitude to Dr. Christiana Dymiotis-Wellington (City University London) for making available to them a large quantity of experimental results, without which this work would not have been possible. The authors also wish to thank Dr. Pedro Tirado (Universitat Politecnica de Valencia) for his collaboration in the Fuzzy Logic applications.

References

[1] Francis AJ, Horman CB, Jerrems LE. The effect of joint thickness and other factors on the compressive strength of brickwork. In: West HWH, Speed KH, editors. Proc. of the 2nd int. brick masonry conf. Stoke-on-Trent, UK: British Ceramic Research Association; 1971. p. 31–7.

[2] Khoo CL, Hendry AW. A failure criterion for brickwork in axial compression. In: Foertig L, Gobel K, editors. Proc., 3rd int. brick masonry conference; 1973. p. 139–45.

[3] Hilsdorf HK. Investigation into the failure mechanism of brick masonry loaded in axial compression. Designing, engineering and constructing with masonry products. Gulf Publishing Company; 1969. p. 34–41.

[4] Binda L, Fontana A, Frigerio G. Mechanical behaviour of brick masonries derived from unit and mortar characteristics. In: Proc. of the 8th international brick/block masonry conf, Dublin; 1988. p. 205–16.

[5] Atkinson RH, Noland JL, Abrams DP. A deformation theory for stack bonded masonry prisms in compression. In: Proc., 7th int. brick masonry conf., Melbourne University, Melbourne; 1982. p. 565–76.

[6] Sarangapani G, Venkatarama Reddy BV, Jagadish KS. Brick-mortar bond and masonry compressive strength. J Mater Civil Eng 2005;17(2):229–37.

[7] Mann W. Statistical evaluation of tests on masonry by potential functions. In: Sixth international brick masonry conference; 1982.

[8] Dayaratnam P. Brick and reinforced brick structures. Oxford and IBH, New Delhi; 1987.

[9] Kaushik HB, Rai DC, Jain SK. Stress–strain characteristics of clay brick masonry under uniaxial compression. J Mater Civil Eng 2007;19(9):728–39.

[10] Dymiotis C, Gutlederer BM. Allowing for uncertainties in the modeling of masonry compressive strength. Constr Build Mater 2007;16(7):1385–93.

[11] Hendry AW, Malek MH. Characteristic compressive strength of brickwork from collected test results. Masonry Int 1986;7:15–24.

[12] ENV 1996-1-1. Eurocode no. 6. Design of masonry structures, Part 1-1: general rules for buildings-rules for reinforced and un-reinforced masonry; 1998.

[13] ACI committee 530. Building code requirements for masonry structure. American Concrete Institute, Farmington Hills, MI; 1999.

[14] Department of transport. The assessment of highway bridges and structures. British Standard BD 21/93, Her Majesty’s Stationery Ofc., London; 1993.

[15] Mansour MY, Dicleli M, Lee JY, Zhang J. Predicting the shear strength of reinforced concrete beams using artificial neural networks. Eng Struct 2004;26(6):781–99.

[16] Caglar N. Neural network based approach for determining the shear strength of circular reinforced concrete columns. Constr Build Mater 2009;23(10):686–91.

[17] Oreta AWC. Simulating size effect on shear strength of RC beams without stirrups using neural networks. Eng Struct 2004;26(5):681–91.

[18] Kumar S, Barai SV. Neural networks modeling of shear strength of SFRC corbels without stirrups. Appl Soft Comput 2010;10(1):135–48.

[19] Dahou Z, Sbartaı¨ ZM, Castel A, Ghomari F. Artificial neural network model for steel-concrete bond prediction. Eng Struct 2009;31(8):1724–33.

[20] Fujitani H, Midorikawa M, Iiba M, Kitagawa Y, Miyoshi T, Kawamura H, Tani A, Mochio T. Seismic response control tests and simulations by fuzzy optimal logic of building structures. Eng Struct 1998;20(3):164–75.

[21] Kim YM, Kim CK, Hong SG. Fuzzy based state assessment for reinforced concrete building structures. Eng Struct 2006;28(9):1286–97.

[22] Mashrei MA, Abdulrazzaq N, Abdalla TY, Rahman MS. Neural networks model and adaptive neuro-fuzzy inference system for predicting the moment capacity of ferrocement members. Eng Struct 2010;32(6):1723–34.

[23] Anoop MB, Rao KB, Rao TVRSA. Application of fuzzy sets for estimating service life of reinforced concrete structural members in corrosive environments. Eng Struct 2002;24(9):1229–42.

[24] McNary WS, Abrams DP. Mechanics of masonry in compression. J Struct Eng 1985;111(4):857–70.

[25] Naraine K, Sinha S. Behaviour of brick masonry under cyclic compressive loading. J Struct Eng 1989;115(6):1432–45.

[26] Rai DC, Goel SC. Seismic strengthening of unreinforced masonry piers with steel elements. Earthquake Spectra 1996;12(4):845–62.

[27] Hendry AW. Structural masonry. London: Macmillan Press; 1998.

[28] Tomazevic M. Earthquake resistant design of masonry buildings. London: Imperial College Press; 1999.

[29] Sarangapani G, Reddy BV, Jagadish KS. Structural characteristics of bricks, mortars and masonry. J Struct Eng 2002;29(2):101–7.

[30] Berto L, Saetta A, Scotta R, Vitaliani R. Failure mechanism of masonry prism loaded in axial compression: computational aspects. Mater Struct 2005;38(2):249–56.

[31] Ewing BD, Kovalsky MJ. Compressive behavior of unconfined and confined clay brick masonry. J Struct Eng 2004;130(4):650–61.

[32] Brencich A, Gambarotta L. Mechanical response of solid clay brickwork under eccentric loading. Part I: Unreinforced Masonry. Mater Struct 2005;38(2):257–66.

[33] Roberts TM, Hughes TG, Dandamundi VR, Bell B. Quasi-static and high cycle fatigue strength of brick masonry. Constr Build Mater 2006;20(9):603–14.

[34] Chaimoon K, Attard MM. Modeling of unreinforced masonry walls under shear and compression. Eng Struct 2006;29(9):2056–68.

[35] Corradi M, Grazini A, Borri A. Confinement of brick masonry columns with CFGRP materials. Compos Sci Technol 2007;67(9):1772–83.

[36] Brencich A, Corradi C, Gambarotta L. Eccentrically loaded brickwork: theoretical and experimental results. Eng Struct 2008;30(12):3629–43.

[37] Brencich A, de Felice G. Eccentric loading of solid clay brickwork: experimental results and macroscopic models. Constr Build Mater 2009;23(5):1935–46.

[38] Prakash SS, Alagusundaramoorthy P. Load resistance of masonry wallettes and shear triplets retrofitted with GFRP composites. Cem Concr Compos 2008;30(8):745–61.

[39] Zhou Z, Walker P, D’Ayala D. Strength characteristics of hydraulic lime mortared brickwork. Proc ICE – Constr Mater 2008;161(4):139–46.

[40] Matlab 7.0. User’s Guide. The MathWorks, Inc., Natick, MA, 2004.

[41] Zadeh LA. Fuzzy sets. Inform Control 1965;8:338–53.