Figure 1. In-situ growth method scheme for LDH conversion coatings on the 2024-T3 alloy.

Figure 2. Surface appearance and optical profilometry micrographs of (a) Ca-Al-LDH and (b) Ca-Al-LDH-Mn coatings, including the 2D-real colour images and 3D-topographical maps.

Figure 3. Planar view (a-d) and cross-sectional view (e, f) of secondary electron micrographs of Ca-Al-LDH and Ca-Al-LDH-Mn coatings on 2024 alloy.

Figure 4. XRD patterns of Ca-Al-LDH and Ca-Al-LDH-Mn coatings on 2024 alloy.

Figure 5. Transmission electron micrographs of (a) Ca-Al-LDH and (b) Ca-Al-LDH-Mn coatings on 2024-T3 alloy.

Figure 6. FTIR spectra of Ca-Al-LDH and Ca-Al-LDH-Mn coatings on 2024 alloy.

Figure 7. Survey XPS spectra of (a) Ca-Al-LDH and (b) Ca-Al-LDH-Mn coatings.

Figure 8. High-resolution XPS spectrum of Mn 2p for Ca-Al-LDH-Mn coating.

Figure 9. Bode plots of the Ca-Al-LDH and Ca-Al-LDH-Mn coatings after 1 hour and 28 days of immersion time in 3.5 wt. % NaCl solution.

Figure 10. Equivalent circuit used to fit the EIS data of Ca-Al-LDH and Ca-Al-LDH-Mn coatings grown on AA2024-T3 substrate after 1 hour and 28 days of immersion in 3.5 wt. % NaCl solution.

Figure 11. Water drop and surface appearance of painted LDH coatings surfaces after the paint adhesion test. Rating 0 for both Ca-Al-LDH and Ca-Al-LDH-Mn.

Figure 12. Surface appearance of Ca-Al-LDH and Ca-Al-LDH-Mn scribed coatings following immersion in 3.5 wt. % NaCl solution at different time points. Red arrows indicate the corrosion damage.

Figure 13. Scanning electron micrographs corresponding to the scribed plan views of Ca-Al-LDH and Ca-Al-LDH-Mn coatings (a) before the test and (b) after 7 days of immersion in 3.5 wt. % NaCl solution. Note that in each case EDS analyses have been performed of the general area comprising the scribe (1), inside the scribe (2), and of the coating outside the scribe (3).

Figure 14. Schematic diagram of the active corrosion protection mechanism for the Ca-Al-LDH-Mn system (3.5 wt. % NaCl solution at pH 6.6 ± 0.2).