Table 1. Examples of corrosion studies on inhibitor-loaded LDH coatings grown on AA2024-T3 by the in situ method.

| LDH Recipe/conditions | Post-treatment/Thickness | Corrosion | Ref |
| --- | --- | --- | --- |
| Mg/Al-LDH 0.038 M MgSO4 0.075 M Al2(SO4)3 0.595 M H2NCONH2 (90-120) ºC; 9h. | - Vanadate-loading: 24 h in 0.38 M Vanadate solution (No T data, pH: 4.5-5.5). - Sol-Gel coating - Thickness: LDH-V/Sol-gel: 5.8µm. | ¦Z¦10 mHz (Ω·cm2) in 3.5 wt. % NaCl - LDH/Sol-gel: 104 (0.5 h) and 4·104 (24-480) h - LDH-V/Sol-gel: ̴ 105 (0.5-480) h | [19] |
| Zn/Al-LDH Zn(NO3)2 solution pH: neutral range < 100 ºC; Few hours. | - Vanadate-loading: Immersion in NaVO3 solution (no concentration data) (< 50 ºC and pH: 8-9). - Thickness: LDH-V: 3-7 µm | ¦Z¦10 mHz (Ω·cm2) in 2.9 wt. % NaCl Unsealed: 4·103 (25 min); 104 (720h) LDH: 1·106 (25 min); 105 (720h) LDH–V: 3·105 (25 min); 2·105 (720h) | [18] |
| Zn/Al-LDH 0.005 M Zn(NO3)2 pH: neutral range < 100 ºC; 168-300 h. | - Vanadate-loading: Immersion in NaVO3 solution (no concentration data) (< 50 ºC and pH: 8-9). For a few hours. - Thickness: No data | ¦Z¦10 mHz (Ω·cm2) in 2.9 wt. % NaCl Zn-Al-LDH: 105 (168 h); 103 (350 h) Zn-Al-LDH-V: 7·105 (700 h) | [20] |
| Zn/Al–LDH 0.05 M Zn(NO3)2 0.3 M NH4NO3 45 ºC, 6 h; pH: neutral. | 1- Vanadate-loading: Immersion in 0.1 M NaVO3 (pH: 8.8 ± 0.2). 2- Molybdate-loading: Immersion in 0.1 M Na2MoO4 (pH: 8.8 ± 0.2). 3- MBT-loading: Immersion in 0.1 M NaMBT solution (pH:10). All reactions were performed at 45ºC and 2 h. -Thickness: No data | PDP (Ecorr (V); icorr (A·cm-2)) in 2.9 wt. % NaCl Unsealed: -0.55; 1.04·10-5 Zn-Al-LDH: -0.51; 4.2·10-6 Zn-Al-LDH-V: -0.46; 9.44·10-8 Zn-Al-LDH-Mo: -0.50; 5.25·10-7 Zn-Al-LDH-MBT: -0.45; 5.57·10-7 | [21] |
| Zn/Al/Ce-LDH: 0.05 M Zn(NO3)2 0.005 M Ce(NO3)3 0.3 M NH4NO3 - 70 ºC; 24 h. | -Vanadate-loading: Immersion in 0.1 M NaVO3 solution (45 ºC and pH: 8.8 ± 0.2). For 2 hours. - Thickness: ZnAlCe/V2O7: 2 µm | ¦Z¦10 mHz (Ω·cm2) in 2.9 wt. % NaCl ZnAl-NO3: 4·103 (24 h), ZnAlCe-NO3: 104 (24 h) ZnAlCe/ V2O7: 106 (24 h); 2·106 (336 h) | [22] |
| Zn/Al-LDH: 0.05 M Zn(NO3)2 0.3 M NH4NO3 - 45 ºC, 6 h; pH: neutral. | - Molybdate-loading: Immersion in 0.1 M Na2MoO4 (45 ºC and pH: 10). For 2 hours. - Thickness: 1. LDH-MoO4: 15.605 nm 2. LDH-MoO4/GN: 12.217 nm | ¦Z¦10 mHz (Ω·cm2) in 3.5 wt. % NaCl LDH-MoO4: 4·104 MoO4/GN: 2·105 | [23] |

Table 2. Roughness values of studied Ca-Al-LDH-based coatings on 2024.

| Roughness (µm) | Ca-Al-LDH | Ca-Al-LDH-Mn |
| --- | --- | --- |
| Ra Sa | 0.10±0.01 0.30±0.02 | 0.30±0.02 0.40±0.02 |

Table 3. EDS (at. %) area analysis of Ca-Al-LDH and Ca-Al-LDH-Mn coatings on 2024 alloy.

| Coating | Location |  | O | Al | Ca | Mn | Cu | Mg | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca-Al-LDH | Longitudinal view | 1 | 55.6 | 43.0 | - | - | 0.3 | 1.0 | 0.1 |
|  |  | 2 | 65.2 | 33.4 | 0.1 | - | 0.6 | 0.4 | 0.3 |
|  |  | 3 | 70.0 | 29.1 | 0.1 | - | 0.3 | 0.3 | 0.2 |
|  | Cross-section view | 4 | 52.8 | 45.3 | 0.1 | - | 1.0 | 0.8 | - |
|  |  | 5 | 56.2 | 43.0 | - | - | 0.2 | 0.6 | - |
| Ca-Al- LDH-Mn | Longitudinal view | 1 | 46.4 | 52.0 | - | 0.4 | 0.4 | 0.8 | - |
|  |  | 2 | 84 | 5.5 | 0.5 | 9.2 | - | 0.3 | 0.5 |
|  |  | 3 | 69.4 | 21.1 | 0.2 | 2.0 | 5.3 | 1.8 | 0.2 |
|  | Cross-section view | 4 | 68.1 | 29.8 | 0.3 | 1.0 | 0.2 | 0.5 | 0.1 |
|  |  | 5 | 24.6 | 64.7 | - | 1.0 | 6.5 | 0.2 | 3.0 |

Table 4. XPS results of Ca-Al-LDH and Ca-Al-LDH-Mn coatings. Note that K was deliberately not included in the Ca-Al-LDH-Mn.

| Element | Binding energy (eV) | at. % |
| --- | --- | --- |
| Ca-Al-LDH |  |  |
| O 1s | 531.8 | 52.4 |
| C 1s | 287.7 | 20.9 |
| Ca 2p | 349.9 | 2.8 |
| Al 2p | 75.3 | 23.9 |
| Ca-Al-LDH-Mn |  |  |
| O 1s | 531.0 | 57.0 |
| C 1s | 287.1 | 10.4 |
| Ca 2p | 349.1 | 1.3 |
| Al 2p | 74.4 | 19.8 |
| Mn 2p | 641.7 | 11.5 |

Table 5. XPS results for the Mn 2p level in the Ca-Al-LDH-Mn coating. Note that the total Mn content in the analysed surface amounts to 11.5 at.%.

| Mn oxidation state | Binding energy (eV) | Peak area (%) | at. % |
| --- | --- | --- | --- |
| Mn+2 | 640.5 | 29.1 | 3.3 |
| Mn+3 | 641.7 | 32.6 | 3.8 |
| Mn+4 | 643.0 | 30.6 | 3.5 |
| Mn+7 | 646.8 | 7.7 | 0.9 |

Table 6. Equivalent circuit data for Ca-Al-LDH and Ca-Al-LDH-Mn on 2024 alloy in 3.5 wt. % NaCl solution. The standard deviation values are shown in parentheses.

| Coating | CPE LDH-out (F s(n-1)·cm-2) | n LDH-out | R LDH-out ( cm2) | CPE LDH-in (F s(n-1)·cm-2) | n LDH-in | R LDH-in ( cm2) | CPEdl (F s(n-1)·cm-2) | ndl | Rp ( cm2) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 hour |  |  |  |  |  |  |  |  |  |
| Ca-Al-LDH | 8.7·10-6 (±1·10-6) | 0.82 | 21 (±2) | 4.9·10-6 (±1·10-6) | 0.91 | 1.7·104 (±1·103) | 1.6·10-4 (±2·10-5) | 0.93 | 5.6·104 (±1·103) |
| Ca-Al-LDH-Mn | 9.5·10-6 (±1·10-7) | 0.84 | 450 (±40) | 1.1·10-7 (±1·10-9) | 0.98 | 2.9·105 (±1·104) | 5.7·10-6 (±1·10-6) | 0.80 | 5.2·105 (±1·102) |
| 28 days |  |  |  |  |  |  |  |  |  |
| Ca-Al-LDH | 9.7·10-6 (±6·10-7) | 0.96 | 13 (±4) | 6.1·10-5 (±6·10-6) | 0.78 | 9.1·103 (±4·102) | 1.4·10-3 (±2·10-4) | 0.84 | 1.1·104 (±2·102) |
| Ca-Al-LDH-Mn | 7.9·10-6 (±5·10-6) | 0.85 | 80 (±30) | 8.4·10-6 (±5·10-7) | 0.77 | 5.9·104 (±1·103) | 3.3·10-4 (±1·10-5) | 0.77 | 7.1·104 (±4·103) |

Table 7. EDS (at. %) area analysis of scribed Ca-Al-LDH and Ca-Al-LDH-Mn coatings on 2024 alloy before and after 7 days of immersion in 3.5 wt. % NaCl solution.

| Coating | Location |  | C | O | Mg | Al | Ca | Cu | Mn |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca-Al-LDH | Before test | 1 | 34.0 | 18.0 | 0.7 | 46.2 | 0.1 | 1.0 | - |
|  |  | 2 | 36.7 | 4.0 | 0.9 | 57.4 | - | 1.0 | - |
|  |  | 3 | 27.8 | 19.0 | 0.7 | 50.5 | 0.2 | 1.8 | - |
|  | After 7 days | 1 | 22.5 | 46.1 | 0.4 | 30.2 | - | 0.8 | - |
|  |  | 2 | 17.3 | 50.0 | - | 30.2 | - | 2.5 | - |
|  |  | 3 | 19.6 | 47.0 | 0.3 | 32.2 | - | 0.9 | - |
| Ca-Al- LDH-Mn | Before test | 1 | 30.6 | 21.8 | 0.7 | 45.5 | - | 0.9 | 0.5 |
|  |  | 2 | 28.3 | 4.7 | 1.1 | 64.6 | - | 1.3 | - |
|  |  | 3 | 21.6 | 24.2 | 0.7 | 50.5 | - | 1.9 | 1.1 |
|  | After 7 days | 1 | 22.9 | 45.3 | 0.4 | 30.4 | - | 0.8 | 0.2 |
|  |  | 2 | 16.8 | 40.0 | 0.5 | 41.6 | - | 0.8 | 0.3 |
|  |  | 3 | 19.0 | 25.5 | 0.8 | 53.5 | - | 1.0 | 0.2 |