Table 1. Composition (at.%) of the AZ31B magnesium alloy coated with PCC. EDS locations are labelled in Figure 3b.

| PCC | O | Mg | Al | P | Ca | Mn | Zn |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S1-Outer layer | 67.2 | 1.2 | - | 15.3 | 2.8 | 4.9 | 8.6 |
| S2-Inner layer | 70.8 | 25.5 | 3.1 | - | - | 0.1 | 0.5 |
| S3-Substrate | 4.8 | 92.3 | 2.3 | - | - | 0.2 | 0.4 |

Table 2. EDS results (at.%) for the studied Flash-PEO coatings. EDS locations are labeled in Figure 5.

|  | O | F | Mg | Al | Si | P | K | Ca | Mn | Zn |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SiF |  |  |  |  |  |  |  |  |  |  |
| S1-Top Layer | 55.5 | 1.4 | 28.2 | 1.7 | 13.1 | - | - | - | 0.1 | - |
| S2-Intermediate Layer | 52.0 | 4.0 | 30.6 | 1.3 | 11.6 | - | 0.1 | - | 0.2 | 0.2 |
| S3-Barrier Layer | 31.8 | 12.4 | 49.6 | 2.0 | 3.7 | - | - | - | 0.2 | 0.3 |
| PCC-SiF |  |  |  |  |  |  |  |  |  |  |
| S1-Top Layer | 58.2 | - | 12.3 | 4.2 | 6.7 | 5.6 | 1.7 | 1.4 | 4.4 | 5.5 |
| S2-Intermediate Layer | 48.3 | 9.1 | 32.8 | 2.4 | 6.7 | 0.2 | 0.2 | - | 0.1 | 0.2 |
| S3-Barrier Layer | 31.7 | 7.3 | 55.3 | 2.7 | 2.4 | 0.2 | - | - | - | 0.4 |
| SiPF |  |  |  |  |  |  |  |  |  |  |
| S1-Top Layer | 56.8 | 4.1 | 28.5 | 1.9 | 5.9 | 2.7 | - | - | 0.1 | - |
| S2-Intermediate Layer | 46.3 | 7.4 | 36.7 | 1.5 | 4.3 | 3.3 | 0.2 | - | 0.1 | 0.2 |
| S3-Barrier Layer | 31.8 | 15.3 | 48.0 | 1.9 | 1.6 | 1.1 | - | - | 0.1 | 0.2 |
| PCC-SiPF |  |  |  |  |  |  |  |  |  |  |
| S1-Top Layer | 61.1 | - | 17.5 | 2.5 | 1.8 | 10.3 | 1.6 | 0.7 | 1.6 | 2.7 |
| S2-Intermediate Layer | 51.0 | 7.8 | 32.8 | 2.7 | 3.3 | 1.9 | 0.2 | - | - | 0.2 |
| S3-Barrier Layer | 31.1 | 13.3 | 50.5 | 2.2 | 1.5 | 1.1 | - | - | - | 0.3 |

Table 3. Pore diameter for the studied PEO coatings.

|  | SiF | SiPF | PCC-SiF | PCC-SiPF |
| --- | --- | --- | --- | --- |
| D Max [µm] | 5.7 | 5.9 | 16.7 | 13.7 |
| D Avg [µm] | 1.2 ± 0.5 | 1.0 ± 0.4 | 2.3 ± 1.5 | 1.1 ± 0.8 |
| D Min [µm] | 0.6 | 0.6 | 0.6 | 0.6 |
| Porosity [%] | 8.3 | 7.7 | 12.1 | 7.3 |

Table 4. Chemical composition (at. %) of the barrier layer shown in Figure 7.

| O | F | Mg | Al | Si | P | Mn | Zn |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 25.7 | 13.7 | 53.4 | 2.2 | 2.7 | 1.8 | 0.2 | 0.3 |

Table 5. Surface morphology and roughness of the studied systems.

| Sample | Plan View [1 cm2] | Sa* [µm] | S10z** [µm] |
| --- | --- | --- | --- |
| PCC-SiPF |  | 2.5 ± 0.1 | 35.4 ± 2.5 |
| PCC-SiF |  | 2.9 ± 0.1 | 33.6 ± 1.7 |
| SiPF |  | 1.5 ± 0.2 | 21.4 ± 1.0 |
| SiF |  | 1.6 ± 0.0 | 21.0 ± 2.5 |
| PCC |  | 5.8 ± 0.1 | 68.3 ± 4.5 |
| AZ31B |  | 1.7 ± 0.1 | 19.2 ± 0.1 |

* Average height of selected area

** Ten-point height of selected area

Table 6. Contact Angle results for the studied coatings.

| Sample | Contact Angle [°] |  |
| --- | --- | --- |
| PCC-SiPF |  | 0 |  |
| PCC-SiF |  | 20.6 ± 0.4 |  |
| SiPF |  | 28.5 ± 0.4 |  |
| SiF |  | 33.2 ± 0.3 |  |
| PCC |  | 0 |  |
| AZ31B |  | 99.0 ± 0.5 |  |

Table 7. EIS parameters after immersion to 0.5 wt.% NaCl obtained by fitting the impedance diagrams using equivalent circuits with one or two time constants.

| System | CPEPCC (Ω-1cm-2sα) | α PCC | RPCC (Ωcm2) |  | CPEdl (Ω-1cm-2sα) | αdl | Rct (Ωcm2) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AZ31B 24h |  |  |  |  | 1.55×10-5 | 0.87 | 4.98×103 |
| AZ31B 96h |  |  |  |  | 2.30×10-5 | 0.78 | 3.64×103 |
| AZ31B 168h |  |  |  |  | 3.23×10-5 | 0.80 | 1.90×103 |
| PCC 24h |  |  |  |  | 2.22×10-5 | 0.80 | 9.38×103 |
| PCC 96h |  |  |  |  | 5.41×10-5 | 0.76 | 3.61×103 |
| PCC 168h | 4.81×10-5 | 0.79 | 5.66×102 |  | 2.98×10-4 | 0.94 | 8.81×102 |
| System | CPEout (Ω-1cm-2sα) | α out | Rout (Ωcm2) |  | CPEin (Ω-1cm-2sα) | αin | Rin (Ωcm2) |
| SiF 24h | 1.13×10-7 | 0.87 | 9.6×104 |  | 7.45×10-8 | 0.96 | 4.82×107 |
| SiF 96h | 2.86×10-7 | 0.83 | 1.16×102 |  | 3.79×10-7 | 0.95 | 1.13×106 |
| SiF 168h | 1.97×10-6 | 0.95 | 1.92×105 |  | 3.08×10-5 | 0.64 | 1.21×105 |
| SiPF 24h | 1.28×10-7 | 0.86 | 1.28×105 |  | 5.36×10-8 | 0.94 | 3.30×108 |
| SiPF 96h | 2.43×10-7 | 0.84 | 4.57×102 |  | 2.35×10-7 | 0.94 | 1.20×106 |
| SiPF 168h | 5.24×10-7 | 0.84 | 9.99×101 |  | 8.15×10-7 | 0.96 | 2.27×105 |
| PCC-SiF 24h | 2.84×10-7 | 0.79 | 3.94×104 |  | 3.68×10-7 | 0.82 | 2.55×106 |
| PCC-SiF 96h | 2.62×10-5 | 0.45 | 5.34×102 |  | 8.18×10-7 | 0.83 | 1.72×103 |
| PCC-SiF 168h | 3.05×10-5 | 0.53 | 1.66×102 |  | 1.22×10-6 | 0.89 | 7.14×103 |
| PCC-SiPF 24h | 3.14×10-7 | 0.76 | 1.58×104 |  | 1.95×10-7 | 0.88 | 1.95×108 |
| PCC-SiPF 96h | 2.61×10-5 | 0.46 | 3.01×102 |  | 5.07×10-7 | 0.90 | 7.58×105 |
| PCC-SiPF 168h | 1.33×10-5 | 0.57 |  | 8.05×101 | 1.34×10-6 | 0.95 | 1.58×103 |  |

Table 8. Visual appearance of the samples by optical microscopy and average |Z|0.01 Hz at 48 h and 168 h of immersion in 0.5 wt.% NaCl. Effective area exposed 1 cm2.

| Sample | 12 h | 48 h | ¦ZI0.01Hz 48 h [Ωcm2] | 168 h | ¦ZI0.01Hz 168 h [Ωcm2] |
| --- | --- | --- | --- | --- | --- |
| PCC-SiPF |  |  | 1.5 x107 |  | 1.8 x 105 |
| PCC-SiF |  |  | 2.8 x 106 |  | 3.9 x 103 |
| SiPF |  |  | 1.9 x 107 |  | 3.6 x 105 |
| SiF |  |  | 6.6 x 106 |  | 3.6 x 105 |
| PCC |  |  | 1.8 x 103 |  | 2.1 x 103 |
| AZ31B Reference |  |  | 3.5 x 103 |  | 9.8 x 102 |